## Slide 1: Decarbonizing Cement
Gernot Wagner. Isabel Hoyos, Camilo Avilés, Jessica Cong, Ariela Farchi, Nicolas Herrera Isaza, Hyae Ryung Kim, Shailesh Mishra, Hoshi Ogawa, Hassan Riaz, Sho Tatsuno, Adele Teh, and Soraya van Beek
16 July 2026
First published: 17 October 2024
Cite as: Wagner et al., “Decarbonizing Cement,” Columbia Business School Climate Knowledge Initiative (16 July 2026).

## Slide 2: Cement and Concrete Industry Overview

## Slide 3
The global cement industry accounts for ~5% to 8% of global CO2 emissions, with partial decoupling from production growth.
  Global cement emissions have more than doubled since 2000 (from 0.7 Gt in 2000 to 1.6 Gt in 2023), while cement output rose ~2.6x.
  Emissions intensity declined ~15% since 2000 (CAGR -0.7%), reflecting efficiency gains.
  China’s share of production fell below 50% in 2023 for the first time in 15 years, while India and Sub-Saharan Africa will drive future demand growth (+42% and +77% by 2030).
Clinker production drives 80% to 90% of cement manufacturing emissions, dominated by calcination and thermal heat:
  ~50% to 60% from limestone calcination and ~30% to 40% from fossil fuel combustion for kiln heat.
  Dry-kiln systems have improved energy efficiency by ~45% compared to wet kilns; over 80% of global production now uses dry kilns.
  Further optimization of kilns and adoption of low-carbon heat sources are key to addressing process emissions.
The industry has been able to reduce emissions intensity by ~17% since the beginning of the century through energy efficiency levers and reduction of the clinker-to-cement ratio.
  The average clinker-to-cement ratio in the U.S. is 0.88 (880 kilograms of clinker per metric ton of cement) as of 2022.
  The global average clinker-to-cement ratio is 0.76, achieved by the increasing share of supplementary cementitious materials (SCMs).
  Portland-limestone cement (PLC) blends up to 15% uncalcined limestone, reducing lifecycle CO2 by ~10%.
  Aging kilns and rising demand present an opportunity to replace or retrofit 15% to 25% of plants over 80 years old, further accelerating reductions in emissions intensity.
Cement and Concrete Industry Overview
Key Messages

## Slide 4: Cement and concrete production account for ~5% to 8% of global CO2 emissions, mostly scope 1
CO2e emissions in 2025: ~55 billion tons
Cement 20%
Chemicals 16%
Non-ferrous Metals 0.2%
Other Industry 37%
Industry
Iron & Steel 27%
Waste 22%
Agriculture, land use, and waste
Livestock 23%
Aviation 10%
Land Use & Forestry 12%
Marine 5%
Crops 38%
Rail 1%
Agriculture fuel 4%
Road 84%
Transport
Power and heat
Commercial Combustion 18%
Oil 2%
F-Gases 36%
Natural Gas 31%
Residential Combustion 46%
Buildings
Coal 67%
Residual 100%
Residuals
22%
23%
18%
15%
8%
13%

## Slide 5: Cement manufacturing emissions are up ~2.2x since 2000, with partial decoupling from production growth (up ~2.6x)
Cement production grew ~2.6x from 2000 to 2015, then stagnated
Emissions-to-production ratio drop suggests efficiency improvements
Cement emissions grew at a lower rate (~2.2x) than production (~2.6x)
Chart: 
 | 1.6 | 2.3 | 3.31 | 4.1 | 4.2 | 4.1
2000
2005
2010
2015
2020
2023
+156.3%
CAGR 6.5%
Chart: 
 | 0.724 | 0.96829 | 1.2631 | 1.4512 | 1.6383 | 1.5693
2000
2005
2010
2015
2020
2023
+116.8%
CAGR +4.7%
Chart: 
 | 45.25 | 42.0996 | 38.1613 | 35.3941 | 39.0476 | 38.3
2000
2005
2010
2015
2020
2023
45.3%
42.1%
38.2%
35.4%
39.0%
38.3%
-15.4%
CAGR -0.7%
Global cement production, billion tons
Global cement manufacturing emissions, GtCO2
Cement emissions-to-production ratio, %

## Slide 6: China has dominated cement production for the past decade, but share expected to decline while emerging markets’ demand grows
China’s production share peaked in 2013, then dipped below 50% of global in 2023 for the first time in 15 years
Demand from emerging markets, led by Sub-Saharan Africa and India, is expected to increase sharply
Chart: 
 | 32.0206 | 29.5664 | 30.4259 | 29.3993 | 28.5115 | 32.6945 | 34.4305
 | 58.3128 | 59.2951 | 57.5412 | 57.5516 | 57.178 | 54.0282 | 49.2537
 | 6 | 6.0841 | 6.5854 | 6.9136 | 8.2195 | 6.8182 | 9.5366
 | 1.9056 | 1.4098 | 1.65 | 2.0121 | 2.5739 | 2.5273 | 2.6085
 | 1.7611 | 1.8971 | 2.0561 | 2.1333 | 2.1268 | 2.0682 | 2.1951
 | 1.7475 | 1.7415 | 1.9901 | 1.3902 | 1.8636 | 1.9756
2%
2011
2013
2015
2017
2019
2021
49%
2023
3.60
4.08
4.10
4.05
4.10
4.40
4.10
2%
-5.2%
Turkey
U.S.
Vietnam
India
China
RoW
Global cement production by country, billion tons
2030 cement demand growth outlook, %
Chart: 
 | 77 | 42 | 39 | 21 | 20 | 15 | 10 | 9 | 1 | 0 | -2 | -28
Sub-Saharan Africa
India
Southwest Asia
LATAM
North America
Southeast Asia
MENA
CIS
Oceania
CEE
Western Europe
East Asia
77%
42%
39%
21%
20%
15%
10%
9%
1%
0%
-2%
-28%
Sources: USGS, Mineral Commodity Summaries (2025); World Cement Association, Industry Outlook (2024).
Credit: Nicolas Herrera Isaza, Isabel Hoyos, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).

## Slide 7: Clinker production is ~85% of cement emissions; dry-kiln adoption has led to significant efficiency gains
Dry kilns have replaced wet kilns for clinker production
1 The production process shown assumes dry-kiln processing, which has widely replaced wet-kiln processing globally.
Sources: Environmental Development, Energy conservation and emission reduction for cement (2022); Portland Cement Association (2024); CEMBUREAU, Cement manufacture fact sheet (2021); Mission Possible, Making net-zero concrete and cement possible (2023).
Credit: Nicolas Herrera Isaza, Jessica Cong, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
Raw meal
Clinker
Concrete
Cement
CaCO3 + heat = CaO + CO2
  Melting clinker
  Precalcining
  Preheat
Vertical cyclones with exhaust gases from the kiln are heated at ~900°C.
Raw meal of crushed limestone and other minerals go in.
Limestone is partially decomposed into lime in a combustion chamber before entering the kiln.
1
2
3
Precalcined meal enters the rotary kiln heated to 1,450°C with fossil fuels combustion.
Clinker is produced.
Chart: 
 | 5.29 | 3.4 | 2.9
Wet kiln
Avg. dry kiln
Optimized dry kiln
-45.2%
-14.7%
Kilns energy efficiency, GJ/t clinker
Observations
Calcination of limestone and combustion of fuels used to bring limestone to the required temperature account for ~90% of clinked production emissions.
The industry is rapidly shifting to adopt dry kilns, with over 80% of global and 90% of European clinker production now using dry kilns. This shift reflects a clear willingness and capacity to change best practices to favor efficiency.
  In dry kilns, raw materials are ground into a fine powder to form a raw meal; in wet kilns, raw materials are mixed with water to form a slurry.
  The wet process is relatively less energy efficient and more resource intensive, with more energy required to evaporate the water in the slurry.
Clinker production is the first step in concrete production1

## Slide 8: Clinker production accounts for over ~85% of cement emissions, of which ~50% are chemical and ~40% thermal
Dry-kiln clinker production process
Concrete breakdown by components and emissions, %
Chart: 
 | 54.0179
 | 20
80.0%
20.0%
Cement
Others
Chart: 
 | 15
 | 85
15.0%
Clinker
SCMs
Chart: 
 | 10
 | 40
 | 50
10.0%
Thermal heat
Limestone reaction
Other
Sources: World Resource Institute, U.S. cement emissions (2024); BBC News, Climate change: The massive CO2 emitter you may not know about (2018).
Credit: Nicolas Herrera Isaza, Isabel Hoyos, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
Observations
Cement is just 15% of concrete mix, yet it accounts for ~80% of the emissions.
Overall, clinker accounts for ~65% to 70% of concrete emissions.
Addressing cement emissions, specifically those related to clinker production, is key to mitigating climate change.
CO2
(Limestone)
(Lime)
CaCO3 + heat → CaO + CO2
→
Ground limestone
CO2 from calcination
Clinker
Hot air
CO2 from heat
Rotating kiln, 1,400℃+

## Slide 9: Clinker production ~85% of cement emissions; lower clinker-to-cement ratio can drive marginal emissions reductions
Clinker-to-cement production process1
Clinker-to-cement ratios vary considerably by region
Observations
Energy emissions from cement grinding account for ~5% of the sector’s emissions.
The higher clinker-to-cement ratio in the U.S. (0.88 versus 0.76 world average) is due to the U.S.’s use of a lower proportion of SCMs than other countries.
Ordinary Portland cement (OPC) can contain up to 95% clinker.
Blended cements, which partially replace clinker with SCMs, are a deployable and cost-effective technology, though they have struggled to gain market share.
Chart: 
 | 0.89 | 0.86 | 0.77 | 0.65
U.S.
Canada
Europe
China
1 The production process shown assumes dry-kiln processing, which has widely replaced wet-kiln processing globally.
Sources: CEMBUREAU, Net-zero roadmap (2024); Portland Cement Association (2024); CEMBUREAU, Cement manufacture fact sheet (2021); Mission Possible, Making net-zero concrete and cement possible (2023).
Credit: Nicolas Herrera Isaza, Jessica Cong, Isabel Hoyos, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
Raw meal
Clinker
Concrete
Cement
  Grinding and blending
  Cooling
Hot clinker is rapidly cooled to 100°C with air blowers powered by electricity.
1
2
Clinker is mixed with 4% to 5% gypsum.
In some cases, it is mixed with other supplementary cementitious materials (SCMs) (e.g., slag, CCR, clay).
The mixture is ground and blended into cement.

## Slide 10: Concrete demand is expected to rise at a ~1.4% CAGR by 2050, driving an increase in absolute cement emissions
Clinker-to-concrete production process1
Concrete demand, billion m3
Observations
Cement is the binding component in concrete and can be used in less or more quantities depending on the strength needed for the end use.
  Cement comprises 10 to 15% of concrete by weight.
Energy emissions from concrete mixing and transportation account for ~5% of the sector’s emissions.
Concrete is usually made at or near a construction site (an average of 50 kilometers away).
Raw meal
Clinker
Concrete
Cement
  Extra additives
  Add aggregates
  Cement + water
Hydration is a chemical process triggered when these are mixed.
It creates heat and a paste-like substance.
Sand and gravel are the ingredients that provide volume in the concrete mix.
The sand fills in tiny spaces, while bigger pieces like gravel or crushed stone fill in larger gaps.
1
2
3
Substances that act as accelerators, retarders, and air-entraining agents alter how the concrete works and improve its performance.
Chart: 
 | 14 | 20
2024
2050
1.4%
1 The production process shown assumes dry-kiln processing, which has widely replaced wet-kiln processing globally.
Sources: GCCA, Societal demand for cement and concrete (2024); Portland Cement Association, Roadmap to Carbon Neutrality (2021); CEMBUREAU, Cement manufacture fact sheet (2021); Mission Possible, Making net-zero cement possible (2023).
Credit: Nicolas Herrera Isaza, Jessica Cong, Isabel Hoyos, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).

## Slide 11: Intensity of U.S. cement emissions has been decreasing; aging plants provide further opportunities to improve efficiency
Observations
Due to new facilities and growing production, emissions have continuously increased at an average 1.3% CAGR since 2010.
The rise of blended cements, fuel shifts from coal to natural gas, and deployment of new and more efficient kilns have reduced emissions intensity by 1% CAGR since 2010.
15% to 25% of plants are 80+ years old and could be replaced or retrofitted for higher efficiency.
  This shift could further reduce emissions intensity, which is projected to reach 0.5 to 0.6 tCO2e/t by 2050.
A significant gap remains between the current global average ( ~0.63) and the IEA’s net-zero by 2030 scenario of 0.45 emissions intensity.
Efficiency gains have reduced the emissions intensity of U.S. cement production; emissions from new plants are projected to continue increasing due to growing demand
Chart: 
 | 20.5174 | 22.567 | 23.5348 | 24.2475 | 25.6498 | 25.6875 | 25.6665 | 24.8654 | 25.646 | 25.5295 | 26.5279 | 26.2281 | 23.2876 | 20.9065 | 22.6763 | 23.6488 | 23.933 | 25.0082 | 25.1179 | 25.1825 | 24.2264 | 24.8144 | 24.8687 | 25.8413 | 25.2209 | 22.2687 | 19.6067
 | 13.6783 | 13.8314 | 14.4246 | 14.397 | 12.4585 | 12.1678 | 12.8332 | 12.4327 | 11.8366 | 12.4374 | 12.9238 | 11.2406 | 11.0893 | 9.9555 | 10.0197 | 10.4495 | 10.3347 | 8.8571 | 8.6946 | 9.2013 | 8.852 | 8.4275 | 8.9152 | 9.2639 | 7.9645 | 7.8136 | 6.8796
 | 31.46 | 34.9425 | 36.441 | 40.9177 | 42.5054 | 40.5592 | 40.526 | 41.8786 | 42.0857 | 40.5853 | 42.1725 | 43.7134 | 43.2484 | 46.7908 | 51.6808 | 53.8972 | 59.8326 | 61.4786 | 58.9304 | 59.0821 | 60.5661 | 60.8656 | 59.1219 | 61.434 | 62.8309 | 61.7273 | 65.3558
 | 0.71462 | 0.71119 | 0.71773 | 0.71402 | 0.71402 | 0.68882 | 0.68294 | 0.68424 | 0.68132 | 0.6568 | 0.66974 | 0.66465 | 0.644 | 0.63108 | 0.62805 | 0.63383 | 0.63055 | 0.63055 | 0.6083 | 0.6031 | 0.60426 | 0.60167 | 0.58002 | 0.59145 | 0.58695 | 0.56872 | 0.55731
2024
2030
2035
2040
2045
7
2050
66
79
81
94
94
92
Chart: 
 | 19.7516 | 18.504 | 20.7347 | 21.6239 | 22.7531 | 24.3425 | 24.1904 | 24.054 | 23.474 | 24.4638 | 24.1514 | 25.0958 | 25.1121 | 22.3747
 | 18.811 | 17.6229 | 17.9072 | 18.6752 | 18.7961 | 16.5529 | 16.127 | 16.9269 | 16.5187 | 15.7267 | 16.3884 | 17.0293 | 15.0673 | 14.9165
 | 16.9299 | 19.3852 | 21.6771 | 22.6068 | 25.7209 | 27.2636 | 25.9823 | 25.8357 | 26.9516 | 27.0849 | 25.8765 | 26.8884 | 28.4604 | 28.3413
 | 0.82578 | 0.80921 | 0.80533 | 0.81274 | 0.80853 | 0.80853 | 0.78 | 0.77334 | 0.77482 | 0.77151 | 0.74374 | 0.75839 | 0.75263 | 0.72925
2010
2015
2020
0.73
2023
55
68
66
66
CAGR -1.0%
CAGR +1.3%
Emissions intensity
New (<21y)
Medium (21-50y)
Old (>50y)
U.S. cement plants’ emissions by plant age and overall emissions intensity, MtCO2e and tCO2e/t cement, 2010-2050

## Slide 12: Cement Decarbonization Technologies

## Slide 13
Cement production remains emission intensive, demanding innovation beyond incremental efficiency.
  ~90% of emissions stem from limestone calcination and the high heat needed for clinker production.
Deployable solutions can abate up to ~45% of emissions through efficiency and fuel and clinker substitution.
  Energy efficiency measures are retrofit-ready, delivering ~10% to 15% abatement at negative to low cost (~-$50 /tCO2).
  Alternative fuels such as bioenergy and waste-derived fuels can replace up to 50% of fossil fuels.
  Substituting clinker with SCMs and LC3 can reduce emissions by ~15% to 40%, with modest process adjustments and cost savings.
Emerging technologies can unlock deep decarbonization but require new infrastructure and capital investments.
  Thermal batteries can replace fossil fuel kilns with electric heat at up to 40% abatement, contingent on low-cost clean electricity.
  Alternative feedstocks and electrochemical production can eliminate up to 90% of process CO2 but face high CapEx and power intensity.
Carbon capture, utilization, and storage (CCUS) serves as a transitional and complementary pathway to retrofit existing assets and reach near-zero emissions.
  Carbon capture can mitigate up to 60% of emissions, serving existing clinker plants and bioenergy systems.
  High costs ($60 to $190/tCO2) and limited storage access constrain adoption, yet CCUS is critical for legacy plants and hard-to-abate clinker lines.
Cement Decarbonization Technologies
Key Messages
Credit: Hoshi Ogawa, Sho Tatsuno, Jessica Cong, Isabel Hoyos, Hyae Ryung Kim, and Gernot Wagner (2025). Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).

## Slide 14: Cost-effective, deployable solutions can partially abate cement emissions; full decarbonization requires emerging technologies
 | Energy efficiency |  | Clinker substitution |  | Alternative production technologies |  |  | Carbon capture
 | Heat optimization | Alternative fuels: Biomass/waste | Blended cement: Traditional SCMs | Blended cement: LC3 | Thermal batteries6 | Alternative feedstock | Electrochemical production | CCUS/CCS
Description | Levers include: Vertical mills or high-pressure grinding rolls Kiln preheaters and improved insulation Waste heat use Digital process control | Using biomass and waste as heat sources can lower thermal emissions: Current kiln heat supply is fossil-fuel dominated (70% coal, 25% oil and gas) | Supplementary cementitious materials (SCMs) Can partially replace clinker in blended cements Include CCR, steel furnace slag, and natural pozzolans | Limestone calcined clay cement (LC3) Blended cement that uses limestone and calcined clay Can replace more clinker than traditional SCMs | High-temperature thermal batteries, powered by cheap electricity, can replace fossil-fueled rotary kilns Can be connected to the grid or powered by off-grid renewables | Non-carbonate rocks can replace limestone as feedstock Can avoid the chemical emissions of limestone calcination | Electrochemistry can break down limestone instead of high-heat kilns Combined with non-carbonate feedstock, it can fully decarbonize cement production | Retrofitting plants with carbon capture can remove CO₂ released during clinker production Captured CO₂ can serve as feedstock, fuels, or building materials
Addressed emissions | Thermal | Thermal | Thermal and chemical | Thermal and chemical | Thermal | Chemical | Thermal | Thermal and chemical
Limiting factor | CapEx | Feedstock availability and cost | Material availability and depletion | Retrofit and CapEx | New tech, CapEx, energy cost | New tech, CapEx | New tech, CapEx, energy cost | High CapEx & OpEx, infrastructure
TRL |  |  |  |  |  |  |  | 
Abatement potential1 | ~9% (2030) ~19% (2050) | ~4% (2030) ~27% (2050) | ~12% (2030) ~39% (2050) | ~8% (2030) ~32% (2050) | ~4% (2030)2 ~12% (2050) | ~4% (2030) ~11% (2050) | ~15-20% (2030)2 ~70-80% (2050) | ~19% (2030) ~69% (2050)4
Abatement cost, $/tCO2e | -46.3/39 (2030) -26.9/14 (2050) | -80/-40 (2030) -25.4/-8 (2050) | -97.7/- 35 (2030) -48.2/- 19 (2030) | -82.7/- 32.2 (2030) -33.2/-11.5 (2050) | 159/414 (2030)3 37/132 (2050) | -44.2/9 (2030)3 -15.4/2 (2050) | 287/593.4 (2030)3 74/152 (2050) | 167/364 (2030)3 46.3/101 (2050)
1Unconstrained theoretical abatement potential for a given ton of cement produced for each approach in isolation. 2Assumes clean energy source. 3Abatement cost of emerging technologies is based on estimates and has high uncertainty. 4Reflects the approximate emissions gap after other measures, not a fixed technical limit. 5Despite TRL9, market penetration remains minimal due to slow standards adoption, limited supply chain coordination, and conservative procurement practices. 6Thermal batteries’ abatement potential and cost are based on off-grid renewables.
Sources: DOE, Pathways to Commercial Liftoff Report (2023); Mission Possible, Net-zero concrete and cement (2023); CATF, Recasting the Future (2025); ACA, Roadmap to Carbon Neutrality (2021); GCCA, Concrete Future (2022); ClimateWorks Foundation, Low-carbon cement (2023); Energies, Alternative Fuels and Energy Efficiency in Cement (2023); International Journal of Greenhouse Gas Control, BioCCS in cement (2023); IEA, Bioenergy Annual Report (2022); RMI, The Business Case for LC3 (2024); Energy Innovation, Industrial Thermal Batteries (2023).
Credit: Camilo Avilés, Nicolas Herrera Isaza, Soraya Van Beek, Isabel Hoyos, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
Mature and commercialized
Pilot plant stage
R&D/Lab stage
Ready for commercialization
5

## Slide 15: Emerging technologies like thermal batteries, alternative feedstock, and electrochemistry are key to achieving full decarbonization
Observations
Currently deployable measures can deliver up to 30% emission reductions through energy efficiency, alternative fuels, and blended cement (conventional SCMs and LC3).
Alternative feedstock and electrochemical production can virtually eliminate cement production emissions but require significant technological advancements and transformational changes to production process.
Thermal batteries' successful deployment depends heavily on low-cost and low-carbon electricity.
Electrochemistry faces challenges including high energy demand and competition for feedstock.
CCS costs vary widely depending on carbon transportation and storage infrastructure.
Abatement cost1 vs. potential2 for key decarbonization pathways by 2030 vs. 2050
500
400
300
200
100
0
600
-100
-200
30%
40%
30%
20%
10%
40%
70%
Abatement potential (%)
70%
Energy efficiency
SCMs
Alt. feedstock
CCUS/CCS5
Alt. fuels
Electrochemical production
LC33
1Abatement cost of emerging technologies is based on estimates and has high uncertainty. 2Abatement potential is calculated as unconstrained and theoretical for each approach in isolation. 3Despite TRL 9, market penetration of LC3 remains low due to slow standards adoption, limited supply chain coordination, and conservative procurement practices. 4Thermal batteries' abatement potential and cost are based on off-grid renewables; see slide 25 for grid power. 5CCUS/CCS calculations reflect the approximate emissions gap after other measures, not a fixed technical limit.
Sources: DOE, Liftoff Report (2023); Mission Possible, Net-zero concrete and cement (2023); CATF, Recasting the Future (2025); ACA, Roadmap to Carbon Neutrality (2021); GCCA, Concrete Future
(2022); ClimateWorks Foundation, Low-carbon cement (2023); Energies, Alternative Fuels and Energy Efficiency in Cement (2023); International Journal of Greenhouse Gas Control, BioCCS in cement (2023); IEA, Bioenergy Annual Report (2022); RMI, The Business Case for LC3 (2024); Energy Innovation, Industrial Thermal Batteries (2023).
Credit: Camilo Avilés, Nicolas Herrera Isaza, Soraya Van Beek, Isabel Hoyos, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
Thermal batteries4
500
400
300
200
100
0
600
-100
-200
Abatement cost ($/tCO2e)
10%
10%
10%
5%
10%
20%
Abatement potential (%)
20%
5%
Electrochemical production
CCUS/CCS5
Thermal batteries4
Alt. fuels
SCMs
LC33
Energy efficiency
Alt. feedstock
2030
2050

## Slide 16: Currently deployable energy efficiency measures can cut ~10% to 15% of cement production emissions through plant retrofits
Observations
Energy efficiency measures improve how energy is consumed rather than changing cement chemistry.
The measures address both electricity and thermal demand: Grinding and motors reduce indirect emissions, while kiln upgrades and waste heat recovery cut fuel-related emissions.
Most levers are retrofit-friendly, meaning most plants can implement them without rebuilding kilns, making them the fastest abatement option compared with SCMs or CCUS.
Process control and high-efficiency motors deliver largest abatement at easiest installation
Abatement potential of energy efficiency levers, 2023-50, MtCO2/year
Chart: 
 | 50.5495
 | 28.5714
 | 10.989
 | 9.8901
50%
By 2050
~200 (100%)
Lever | Energy source | TRL 1-10 | Retrofit or new | Ease of installation | Scalability | Co-benefits
Grinding optimization1 | Electricity | 9 | Retrofit | Medium – major retrofit | High (all plant sizes) | Lower costs, finer product
Waste heat recovery2 | Both | 7-8 | Retrofit | Medium – add-on unit | Medium (needs large scale) | On-site power, energy security
Process control & optimization3 | Electricity | 9 | Retrofit | High – plug & play | Very high (all plants) | Stable ops, lower maintenance
Kiln upgrades4 | Thermal | 8-9 | Retrofit and new | Low – very disruptive | High (large plants best) | Higher output, fuel flexibility
Abatement potential is expected to stay constant through 2050, as measures are already highly mature, with limited future efficiency gains. Impact is front loaded because potential can be realized now.
Grinding
Waste Heat Recovery
Process Control & Optimization
Kiln Upgrades
Energy efficiency

## Slide 17: Share of bioenergy for heating kilns is expected to increase, as large producers set targets to shift away from fossil fuels
Observations
Coal dominates cement production fuel use at 70%, followed by oil and natural gas at 24%. Alternative fuels (biomass, waste) account for just 5%.
Switching to bioenergy fuels that are less carbon intensive than conventional fuels can deliver reductions of ~200 MtCO2, or 14% of the cumulative cement CO2 emissions savings, by 2050 under IEA 2°C — assuming 100% abatement of fuel emissions by bioenergy and an additional 20% process emissions abatement.
Industry pilots are diversifying the alternative fuel mix: Heidelberg Materials is testing hydrogen/ammonia as fuel carriers to decarbonize kiln heat, while Cemex has produced solar clinker with concentrated solar heat (1,500°C+) and is scaling toward continuous industrial operation.
Replacing fossil fuels with bioenergy has an abatement potential of ~200 MtCO2/year but varies widely by biomass type
Chart: 
 | 95 | 72 | 50 | 14
 | 5 | 15 | 17 | 19
 | 0 | 2 | 8 | 19
 | 0 | 10 | 22 | 31
 | 0 | 1 | 3 | 9
 | 0 | 0 | 0 | 8
95%
5%
2022
72%
15%
2%
10%
1%
2030
50%
17%
8%
22%
3%
2035
14%
19%
19%
31%
9%
8%
2050
Chart: 
 | 30 | 29.9 | 37
 | 50 | 45 | 55
30%
50%
30%
45%
37%
55%
2023
2030
While bioenergy is the main alternative fuel in cement, its abatement potential varies widely, as some biomass types emit substantially more carbon than fossil fuels even after biogenic accounting.
Electricity
Hydrogen
Fossil fuels with CCUS
Bioenergy with CCUS
Bioenergy without CCUS
Fossil fuel
Alternative fuels share targets, 2023-30, %
Sources: IEA, Cement NZE guide (2023); International Cement Review, China starts CCUS focus (2024); Heidelberg, First CCS facility in the cement industry (2024); Cemex, Our journey to net-zero (2024); Holcim, Our net-zero journey (2024); Global Efficiency Intelligence, Emissions impact of alternative fuels combustion in cement industry (2023).
Credit: Sho Tatsuno, Jessica Cong, Soraya Van Beek, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
Alternative fuels

## Slide 18: Cement kiln bioenergy deployment requires low CapEx, with abatement costs expected to drop ~20% to 45% by 2050
Observations
Bioenergy with CCS: Current abatement costs are high (≈$157-$193/tCO₂ in 2023), but learning and scaling can reduce them by ~45% by 2050 (≈$89-$107/tCO₂). Costs are dominated by CCS infrastructure (capture, compression, storage) rather than the fuel itself.
Bioenergy without CCS: Costs are already very low (≈$11-$15/tCO₂ in 2023), driven by RDF/SRF gate fees and existing infrastructure. Modest improvements reduce costs further, by ~20% to ≈$9-$12/tCO₂ by 2050.
Policy dependence: Deployment depends heavily on landfill and waste regulations (to supply RDF/SRF), carbon pricing (to value abatement), biomass sustainability rules, and public support for CO₂ transport and storage networks.
Alternative fuels + CCS
Chart: 
 | 11 | 8.8
 | 4 | 3.2
2023
2050
15.0
12.0
-20.0%
Chart: 
 | 157 | 89
 | 36 | 18
2023
2050
193.0
107.0
-44.6%
Conservative scenario
Optimistic scenario
Conservative scenario
Optimistic scenario
Abatement cost for bioenergy with CCS, 2023-50, $/tCO2
Abatement cost for bioenergy without CCS, 2023-50, $/tCO2
Main fuels: RDF, SRF, and biomass residues (wood waste, agricultural by-products, sewage sludge).
Already commercial (TRL 8-9), widely used in Europe.
Costs shaped by logistics, pre-treatment, and kiln retrofits; gate fees often make RDF/SRF very low-cost or even negative-cost fuels.
Can abate up to 100% of thermal emissions.
Combines biofuels (incl. RDF/SRF, residues, energy crops) with CO₂ capture at kilns, tackling both fuel and process emissions.
Costs are driven by biomass supply and CCS CapEx/OpEx (capture, compression, storage).
Biomass use is commercial, but CCS in cement is at pilot scale (TRL ~6-7); storage infrastructure is at <1% of 2050 needs.
Enables near-complete or even net-negative thermal emissions.
Bioenergy with CCS
Bioenergy without CCS
Bioenergy with CCS is capital intensive but offers potential negative emissions

## Slide 19: Blended cements partially replace clinker, reducing emissions with minor changes to production process or added costs
Observations
Global clinker production is ~3.8 Gt/year. Replacing 50% of global clinker would require SCM supply far above today’s ~500 to 600 Mt/year of usable materials; only LC3 offers long-term, scalable supply.
At the product level, furnace slag has the potential to replace up to 50% of clinker, but global availability limits slag-based substitution.
Coal combustion residuals (CCR) cements can substitute 30% to 35% at the plant level but globally only ~10% to 20% due to limited supplies of high-quality CCR as coal plants retire.
LC3 can deliver 30% to 40% clinker reduction, but current industrial capacity is small (~1% to 2% of global cement) and significant new calcination and production infrastructure is required.
 | Clinker | Furnace slag (GGBFS) | Coal combustion residuals (CCR) | Calcined clay (LC3)
Replacement potential | N/A | 30-50%1 | 30-35% | 30-40%
Availability | 3.8 billion Mtpa | 520-680 Mtpa | 500-800 Mtpa | 3.5-5 Mtpa
Availability-adjusted replacement potential | N/A | ~10-18% | ~10-20% | 1-2%
Emissions reduction potential2 | N/A | ~15-30% | ~15-30% | ~30-40%
Price $/ton | ~65-75 | ~51 | ~45 | ~20-35
Blended cements
-20
-15
-10
-5
0
-25
30%
30%
-14
-20
-22
31.6%
Abatement cost3 ($/tCO2e) vs. emission abatement potential (% tCO2e)
1 30% to 50% replacement in CEM II/B-S or CEM III/A; up to 60% to 70% in CEM III/B. 2 The % CO2 reduction achieved if the full technical replacement potential is used. 3 Cost relative to clinker.
Sources: CKI analysis; DOE, Liftoff Report (2023); RMI, The business case for LC3 (2024); IEA, Net Zero by 2050 (2023); GCCA, Concrete Future Roadmap (2021).
Credit: Nicolas Herrera Isaza, Isabel Hoyos, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).

## Slide 20: Reducing clinker ratios is a high priority for cement companies, but more support is needed to reach the IEA target of 0.57 by 2050
Observations
Except for Heidelberg, major cement manufacturers’ 2030 targets lag behind the IEA 2030 net-zero scenario.
Based on historical trends, reaching IEA’s 2030 and 2050 targets will require more aggressive clinker ratio reductions.
This lag may be reflective of certain constraints:
  Limited availability of traditional SCMs as by-products decline. Cement manufacturers have historically relied on by-products such as coal combustion residuals (CCR) and blast furnace slag to reduce the clinker ratios. The phasing out of coal-fired power plants and decarbonization of the steel industry has reduced the ready supply of such by-products.
  Scalability issues of new SCMs. Newer SCMs like calcined clay and natural pozzolans show promise, but scaling up their production presents challenges, as supply chain infrastructure for these alternatives is still relatively immature.
  Need for policy support. Stronger global policy and standardization are required to push the global clinker ratio onto the IEA net-zero trajectory.
  Performance trade-offs and market hesitancy around newer blends. High-blend cements, which use significant amounts of SCMs, can exhibit slow early-age strength development and raise uncertainty about long-term durability. Even if structural integrity is unaffected, it may be challenging to win regulatory and customer approval and acceptance.
Sources: IEA, Cement (2023); Congressional Research Service, Cement (2023); Heidelberg, 2024 Annual Report (2025) and Capital Markets Day (2025); Cemex, 2024 Annual Report (2024); Holcim, 2024 Annual Report (2024); IEA Net Zero by 2050 (2021); RMI, Unleashing the Potential of LC3 (2023); International Cement Review, SCMs: Environmental and Qualitative Benefits (2022). Credit: Adele Teh, Hoshi Ogawa, Sho Tatsuno, Isabel Hoyos, Jessica Cong, Shailesh Mishra, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
Chart: 
 | 0.66 | 0.67 | 0.68 | 0.7 | 0.71 | 0.71 | 0.7 | 0.71 | 0.65 | 0.57
2015
2016
2017
2018
2019
Clinker factor, global average, 2015-50
2021
2022
2030
2050
2020
IEA net-zero scenario
Forecast
Clinker reduction
Chart: 
 | 71.7 | 69 | 71
 | 68 | 64 | 68
0.2
0.4
0.6
0.8
0.0
Clinker factor targets, by company, 2023-30
0.68
0.69
0.64
0.71
0.68
0.72
2024
2030
Clinker factor (clinker-to-cement ratio)

## Slide 21: Holcim’s lines of low-carbon cement reduce clinker with SCMs; co-processing plants replace fossil fuels kilns with waste energy
30% less carbon emissions compared with OPC
~14 million tons of waste recycled in 2023
30% of Holcim’s thermal energy from alternative fuels in 2023
Sources: Geocycle, Co-processing (2022); Holcim, Climate report (2023).
Credit: Jessica Cong, Isabel Hoyos, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
Pretreated waste
~1,450°C kiln
Waste ashes become part of the clinker
Raw meal
Clinker
Energy recovery and mineral recycling of pretreated waste
Co-processing
Co-processing is a simultaneous waste recycling and energy recovery process with two primary benefits for cement production:
Sustainable waste management: Co-processing is an alternative to landfills or traditional incineration, as it uses unrecyclable waste. By treating waste at high temperatures, the minerals found in the waste can become part of the clinker.
Fuel alternative for cement kilns: The combustion process provides the heat needed for clinker production and replaces fossil fuel combustion.
Overview
ECOPlanet is a portfolio of low-carbon cement products; ECOPact includes ready-mix low-carbon concrete products.
Holcim’s clinker ratio was 0.72 in 2023.
Company used 10.2% alternative raw materials in 2023.
Carbon reduction technologies
Alternative raw materials: Mixing of supplementary cementitious materials and admixtures.
Mineral components to reduce clinker factor: Recycling construction demolition materials; using innovative materials like calcined clay, pozzolans, and reclaimed ashes; and processing industrial waste.
Calcined clay to replace limestone-based clinker.
Blended cements: Holcim

## Slide 22: Eco Material Technologies produces low-carbon ‘pozzolanic cement’ with SCM of proprietary pretreated CCR
Sources: Pitchbook, Eco Material Technologies (2025); Eco Material, Green cement (2025); Green Cement, Cement alternatives for a greener future (2025); Forbes, Eco Material’s cement is transforming construction (2023); CRH, CRH to Acquire Eco Material Technologies (2025).
Credit: Isabel Hoyos, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
Clinker reduction: Eco Material
Technology
Eco Material Technologies uses a proprietary physical and chemical pretreatment of coal combustion residuals (CCR) — a common pozzolan — that increases its reactivity.
PozzoSlag®, the company’s pozzolanic binding product, can be used as a 50% or higher ordinary Portland cement replacement and is priced the same as unalloyed OPC.
The newest generation of PozzoSlag® can replace up to 100% of OPC in concrete and generates up to 99% less CO2 emissions.
Challenges
CCR is a waste product of coal-fueled power plants, which are being retired across the U.S. and globally.
CCR is produced at coal plants, not where it is needed for construction materials, and its low value makes shipping challenging.
Founded: 2022, Utah, U.S.
Announced acquisition by CRH for $2.1 billion (2025)
According to testing by Eco Material Technologies, PozzoSlag® is 20% stronger than OPC in 28 days and continues to gain long-term strength with time.
Chart: 
 | 2742 | 4092 | 5195 | 5272 | 5827 | 6567
 | 2417 | 4467 | 5367 | 6715 | 6975 | 9217
1
3
7
14
28
56
Control Cement
50% PozzoSlag® / 50% Control Cement
Time (days)
PozzoSlag® can make high-strength, durable concrete
In pounds per square inch
Blended cements: Eco Material

## Slide 23: CalPortland is licensing Solidia’s patent, using carbonation to produce cement that stores CO2
Sources: CalPortland, Solidia licenses low carbon cement (2024); Solidia (2024).
Credit: Isabel Hoyos, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
Blended cements: CalPortland
Licensing agreement: June 2024
H2O and CO2 fill the open spaces between large sand particles and small cement particles.
Cement reacts with CO2 to make calcium carbonate and silica, which harden and make concrete.
Cement powder and sand are mixed and loosely packed.
Licensing agreement
CalPortland entered a patent licensing agreement with Solidia that grants the company limited rights to use its technology and purchase some of its laboratory and plant assets.
Technology
Produces cement with up to 30% less carbon emissions and concrete with up to 50% less emissions.
Uses the same raw materials and equipment as ordinary Portland cement, with a lower proportion of limestone and at lower production temperatures.
The cement gains strength through carbonation — exposure to CO₂ — rather than through hydration, as with OPC. It transforms gaseous CO₂, which may come from industrial emissions, into solid carbonates. This process allows the cement to both utilize and store CO₂.
Blended cements: CalPortland

## Slide 24: Prometheus Materials leverages algae’s natural biomineralization to create a net-zero emissions cement replacement
Sources: CB Insights, Prometheus Materials (2025); Prometheus Materials (2025); Yahoo Finance, Prometheus Completes Landmark Collaboration (2025).
Credit: Ariela Farchi, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
Blended cements: Prometheus
Founded: 2021, Colorado, U.S.
Total funding raised to date: $14.3 million
Chart: 
 | 40 | 60
ProZERO
Cement
104% Reduction in global warming potential (GWP)
Example: Mix Optimized with ProZERO
Technology
Prometheus creates ProZERO® by growing microalgae in large ponds, which naturally biomineralizes and creates limestone organically. After drying, it is treated with a proprietary binder and is then ready to be supplemented into any cement mix.
The natural cycle of microalgae sequesters carbon and avoids the need for mining and kilns.
A mix that blends traditional cement with ~40% of ProZERO can achieve carbon negativity.
Current achievements
Products made using ProZERO’s Ready Mix supplemental blend comply with industry standards for load-bearing and non-load-bearing blocks. Other ProZERO products include Flowable Fill and Manufactured Goods (blocks, pavers, etc.).
Prometheus’ products are estimated to have achieved carbon neutrality in a case study project for a building’s exterior facade in Boulder, CO.
The company signed a landmark agreement to provide ProZERO cement for the construction of New York Climate Exchange’s Campus.

## Slide 25: Thermal batteries can deliver extreme high temperatures powered by electricity, tackling thermal emissions
Heat delivery
Heat generation and storage
Electricity sourcing
Grid power
Off-grid power
Power is bought at market prices (wholesale market or long-term contracts).
Electricity may be from renewables or fossil sources (e.g., natural gas). To achieve decarbonization, it is key to look for cleaner grids.
Prices must be considered, ideally seeking cost-competitive renewable energy deals.
Can be standalone or work in parallel to grid power.
Guarantees greater share of clean energy.
Requires greater capital investment.
Electricity cost may be lower than buying from the grid.
A
B
1
Electric heaters are embedded in a specific medium (e.g., thermal bricks) and heat up to the targeted temperature.
Temperatures can reach up to 1,500°C with current technology.
Thermal radiation can be stored for hours or days. Thermal insulation is key.
2
Air flows through the battery, spreading the stored heat.
Delivery rate can be adjusted by managing air flow.
Air can also be transformed into steam, depending on the industrial needs.
3
2
Hot air or steam can then be delivered steadily at desired temperatures and rates.
A
B
1
3
Sources: RMI, Thermal Batteries (2024); CKI analysis.
Credit: Nicolas Herrera Isaza, Isabel Hoyos, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
Alternative production: Thermal batteries

## Slide 26: Three companies leading thermal battery industry within cement kiln temperature range are at early commercialization stage
Sources: CB Insights, Thermal energy storage developers (2025); Antora (2025); Rondo Energy (2025); Kraftblock (2025); Electrified Thermal Solutions (2025).
Credit: Nicolas Herrera Isaza, Isabel Hoyos, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
Alternative production: Thermal batteries
2020
#
Founding year
2017
2021
2014
2012
Thermal battery model
Temperature range
Storage medium
Commercialization status
Funding and target geographies
Heatcore (HC) and Heatmax (HM)
< 400°C (HC) < 1,500°C (HM)
Carbon blocks
Early commercialization
VC: $200M; Grant: $4M
U.S., Europe
U.S.
bGen ZERO
130-750°C
Crushed rocks
Commercialization
$3.3M valuation, 2022 IPO
Israel → U.S.
Joule Hive Thermal Battery
< 1,800°C
Firebricks
Pilot
VC + Debt: $44M; Grant: $5M
U.S.
U.S.
RHB300
< 1,500°C
Bricks
Early commercialization
VC: $82M
U.S., Middle East, Asia
U.S.
Net-Zero Heat System
< 1,300°C
Not disclosed
Early commercialization
VC: $22M; Grant: $2M
EU, U.S.
Germany
Headquarters
Not at cement kiln temperatures yet
Investors

## Slide 27: Brimstone eliminates chemical emissions from traditional cement production by replacing limestone with calcium silicate rocks
Sources: Brimstone (2024); Advanced Research Projects Agency-Energy (ARPA-E) (2024); DOE, Awarded projects: cement and concrete (2024); CB Insights, Brimstone Energy (2025); Business Wire, Amazon and Brimstone collaboration (2025).
Credit: Hoshi Ogawa, Sho Tatsuno, Jessica Cong, Ariela Farchi, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
Alternative production: Brimstone
Founded: 2019, California, U.S.
Total funding raised to date: $72 million
CALCIUM-BEARING SILICATE ROCK
PORTLAND CEMENT
SUPPLEMENTARY CEMENTITIOUS MATERIALS (SCMs)
SMELTER-GRADE ALUMINA
Technology
Brimstone makes cement from carbon-free calcium silicate rocks, eliminating the calcination process, which accounts for 60% of CO2 emissions in traditional cement production.
Brimstone’s process creates three key co-products: ASTM C150 Portland cement, SCMs, and smelter-grade alumina.
At an industrial scale of production, all three co-products could be sold at competitive market prices.
Current achievements
Advanced in the construction of a commercial-scale plant to produce 140,000 metric tons per year of decarbonized industry-standard ASTM C150 Portland cement, SCMs, and alumina.
Received third-party certification that its cement meets or exceeds ASTM C150 standards for OPC.
Signed a commercial agreement with Amazon, which will reserve annual volumes of Brimstone’s OPC and SCMs, pending successful completion of testing and commercialization to scale up requirements.

## Slide 28: Sublime replaces high-heat kilns with electrochemistry and limestone with alternative feedstocks to reduce ~90% emissions
Technology
Sublime’s technology uses an electrochemical process that replaces carbon-intensive limestone with abundant non-carbonate feedstocks like calcium silicate minerals or industrial waste.
Sublime uses electricity, rather than heat, to break down feedstocks and produce a calcium silica cement, to displace ordinary Portland cement (OPC).
Provides a product that complies with ASTM C1157 standards.
Current achievements
Sublime was planning to build a new, ultralow carbon cement manufacturing facility in Holyoke, Massachusetts — Sublime’s first commercial manufacturing scale-up. However, it paused the plant development in December 2025 after losing a federal grant.
It received an LCA study validating that its cement manufacturing process can reduce 90% of GHG emissions. Sublime’s cement has a GWP1 of 72 kgCO2 /t of cement, while OPC is 922 kgCO2 /ton.
The company signed an agreement with Microsoft for 623K tons over a six- to nine-year period.
Founded: 2020, Massachusetts, U.S.
Total funding raised to date: $53 million
1 GWP: global warming potential.
Sources: Sublime (2025); Advanced Research Projects Agency-Energy (ARPA-E) (2024); DOE, Awarded projects: Cement and concrete (2024); CB Insights, Sublime Systems (2025); Bloomberg News, Microsoft deal for green cements (2025); S&P Global, Sublime pauses Holyoke Plant (2025).
Credit: Hoshi Ogawa, Sho Tatsuno, Jessica Cong, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
Non-carbonate Materials
Electricity
Electrolytic Reactor
Sublime Systems Process
Key emission sources: Limestone, combustion
Coal + limestone = CO2
1 ton OPC = ~1 ton CO2
Electricity + non-carbonate minerals = CO2 avoided
Potential emission sources: Electricity grid mix
Sand, Limestone, Clay
Rotary Kiln
Combustion
Ordinary Portland Cement (OPC) Process
Clinker
Alternative production: Electrochemistry, Sublime

## Slide 29: Furno’s modular, electrified reactors improve efficiency, reduce limestone use, and produce a high-purity CO2 for easier capture
1 XRF: X-ray fluorescence is a non-destructive analytical technique that determines the elemental composition of a sample.
Sources: Pitchbook, Furno (2025); Furno (2024); Business Wire, Furno secures seed funding (2024); TechCrunch, Furno’s super-efficient modular kilns (2024); Cement Products, Furno cement plant concept (2024); Global Cement, Furno Materials ‘low carbon’ cement plant in Chicago (2024).
Credit: Shailesh Mishra, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
Alternative production: Furno
Technology
Modular, high-efficiency mini-kiln: Continuous-flow reactor replaces rotary kilns, with ~80% thermal efficiency and precise temperature control.
Lower-carbon process design: Operates with gas/renewable; uses alternative calcium-rich by-products to cut limestone-related CO2 and produces a high-purity CO2 stream suitable for CCUS.
Current achievements
Funding and deployment: Raised $6.5M seed round and secured a $20M DOE grant to build its first commercial pilot plant.
Product certification: Achieved ASTM C150 cement certification, with independent tests showing ~2x required strength.
Emissions reductions demonstrated: Pilot design shows ~70% fuel-emissions reduction potential and substantial limestone-replacement capability.
Founded: 2020, California, U.S.
Total funding raised to date: $12.4 million
Sourcing raw materials
Passing raw materials through XRF1 spectrometer
Grinding raw meal
Optimizing shape and size
Producing clinker in kiln
Replace the rotary kiln with modular, electrified reactors to improve efficiency and lower CapEx.
Enable decentralized, scalable cement production to reduce transport costs and allow rapid, incremental deployment.
Produce a high-purity CO2 stream to support low-cost carbon capture.
Key strategies
Preheating, calcining, sintering, and cooling in one highly efficient modular reactor

## Slide 30: Carbon capture, utilization, and storage is expected to abate remaining emissions in the cement industry’s path to net zero
CCUS capacity for cement is expected to grow ~9x by 2030
Across scenarios, CCUS is expected to abate 35% to 65% of cement emissions
Observations
As the energy industry continues to phase out fossil fuels, CCUS will play a bigger role in decarbonizing hard-to-abate industries like cement and steel, as opposed to oil and gas.
As of Q1 2025, global CO2 capture and storage capacity in operation reached over 50 Mt. By 2030, capture capacity is expected to reach 430 Mt based on the current project pipeline, with storage capacity at 670 Mt.
Current cement CCUS plants:
  Brevik CCS, Norway (Heidelberg): First industrial-scale CCS cement plant, designed to capture up to 400K tons of CO2 annually. As of May 2025, the plant captured and stored its first 1K tons of CO2.
  Lengfurt Cap2U, Germany (Heidelberg and Linde): First industrial-scale CCU cement plant, designed to capture up to 70K tons of CO2 annually.
Sources: IEA, Net Zero by 2050 (2021); IEA, CCUS Projects Explorer (2025); IEA, Demand and Supply Measures for the Steel and Cement Transition (2025); International Cement Review, China CCUS focus (2024); ICR, China Starts CCUS Focus (2023); Heidelberg, Brevik CCS (2025); GCCA, Concrete Future (2021); MPP, Making Net-Zero Concrete and Cement Possible (2023); PCA, Roadmap to Carbon Neutrality (2024); DOE, Industrial Decarbonization Roadmap (2022); CEMBUREAU, From Ambition to Deployment (2024).
Credit: Adele Teh, Hoshi Ogawa, Sho Tatsuno, Isabel Hoyos, Jessica Cong, Shailesh Mishra, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
Chart: 
 | 63.9 | 18.8
 | 2.7 | 20.8
 | 16.6 | 7.9
 | 6.5 | 11.7
 | 0.5 | 23.7
 | 1.8 | 8
 | 8 | 1
 | 4.7
 | 0.5
 | 2
20
40
60
80
100
0
8%
2%
1%
7%
3%
64%
Operational as of Feb. 2025
2%
1%
5%
1%
8%
24%
12%
8%
21%
19%
Planned by 2030
17%
DAC
Other industry
Chemicals
Iron and steel
Cement
Power and heat
Other fuel transformation
Biofuels
Hydrogen and ammonia
LNG
Chart: 
 | 36 | 38 | 51 | 57 | 65
 | 64 | 62 | 49 | 63 | 35
0
20
40
60
80
100
120
GCCA
MPP
ACA
CEMBUREAU
DOE
100
100
100
120
100
Other levers
CCUS
Operational and planned CCUS capacity by industry, %
Cement abatement from CCUS by roadmap, 2050, %
CCUS

## Slide 31: Oxy-combustion enables high-purity CO2 capture and reshapes CCUS economics for cement
Observations
Purity and concentration improvements mean captured CO₂ can be converted into salable products (e.g., synthetic fuels, building materials), shifting CCUS from a compliance cost to a potential value-generating asset.
The technology can integrate into existing kilns with minimal redesign, enabling rapid, policy-driven deployment and making it especially attractive in markets pursuing state-led decarbonization strategies.
By cutting capture costs by 30% to 50% and pairing well with low-carbon or hydrogen fuels, oxy-fuel CCUS transforms cement capture economics and offers a scalable pathway toward near-zero emissions.
Oxy-combustion boosts flue gas CO₂ concentration from ~15% to >80%, reducing energy required for capture and enabling >95% capture rates with >99.9% purity
Sources: Sina Finance, Sinoma (2025); Sinoma, News (2025); Sinoma, TCDR (2024).
Credit: Anda Wang, Isabel Hoyos, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
An on-site air separation unit (ASU) takes in ambient air and cryogenically separates it, producing high-purity oxygen.
Fuel is burned using pure oxygen and CO₂ gas to create an 80% to 95% concentrated CO₂ exhaust stream.
For the recirculation loop, a large portion is cooled and piped back. For the capture stream, the remaining gas is directed away for final processing.
The captured CO₂ stream is sent to a CO₂ processing unit (CPU). A final product of >99.9% pure liquid CO₂ is ready for transport, utilization, or storage.
Produce pure oxygen
Produce flue gas via oxy-combustion
Split and recirculate flue gas
Purify the final CO2 product
1
2
3
4
CCUS

## Slide 32: CCUS is complementary to near-term solutions but is not a replacement for long-term decarbonization technologies
Observations
CCUS/CCS is a transitional solution that cuts emissions from existing plants and complements other measures, but its role diminishes as other production methods mature.
Opportunities:
  Decarbonize existing cement plants through retrofitting vs. requiring a full rebuild.
  Capture up to ~61%1 of emissions, including unavoidable process CO2 from calcination.
  Reduce costs across multiple sectors by sharing CO2 pipelines and storage hubs.
Challenges:
  Has high CapEx and OpEx cost due to the need for capture units, transport pipelines, and storage infrastructure ($60-$190/t CO2).
  Requires nearby geological storage or CO2 utilization opportunities.
  Depends on regional networks and regulatory support.
CCUS
1 ~60% reflects the approximate emissions gap after other measures, not a fixed technical limit. Realized potential depends on retrofit rates, capture efficiency, and integration with utilization pathways.
Sources: DOE, Liftoff Report (2023); Mission Possible, Making Net-Zero Concrete and Cement Possible (2023); CATF, Recasting the Future (2025); ACM, Roadmap to Carbon Neutrality (2021); GCCA, Concrete Future (2022); ClimateWorks Foundation, Low-carbon cement (2023); Energies, Alternative Fuels and Energy Efficiency in Cement (2023); International Journal of Greenhouse Gas Control, BioCCS in cement (2023); IEA, Bioenergy Annual Report (2022); RMI, The business case for LC3 (2024); Energy Innovation, Industrial Thermal Batteries (2023).
Credit: Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
 | Decarbonization levers | Relevance to CCUS/CCS | Explanation
 | Energy efficiency | Complementary | Efficiency lowers emissions baseline, reducing capture volume and cost per ton.
 | Alternative fuels | Complementary | Fuel switch cuts thermal emissions; CCS can capture remaining process CO2.
 | Blended cements (SCMs/LC3) | Complementary | Blended cements reduce clinker demand and chemical emissions; CCS targets residual emissions.
 | Thermal batteries | Partially substitutable | Electrification cuts combustion emissions; CCS is still useful for process emissions.
 | Alternative feedstocks | Partially substitutable | If feedstock avoids process CO2, CCS becomes less necessary — but may still capture other emissions.
 | Electrochemical production | Largely substitutable | Low-heat, non-carbonate process eliminates need for CCS altogether; there is competition for mineral feedstocks (e.g., calcium, magnesium).
Near term
Long term

## Slide 33: Sinoma's accelerated innovation in China shows that policy-backed R&D can enable technologies like CCUS to scale at speed
CCUS: Sinoma
Sources: Sina Finance, Sinoma (2025); Sinoma, News (2025); Sinoma, TCDR (2024); Sinoma International, Sinoma International Empowering High-Quality Development of Cement Industry - Solutions for Green & Intelligent System (2024).
Credit: Anda Wang, Isabel Hoyos, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
Founded: 1983, Beijing, China
Market cap $5.2 billion
Project highlights
  Massive scale: Captures 200,000 tons of CO₂ per year
  Rapid development: Design completed Dec. 2022 → construction completed Dec. 2023 → commissioned Jan. 2024
Project impacts
  Resource utilization: Captured CO₂ is used for various industrial purposes, including enhanced oil recovery.
  Industry milestone: Represents a significant step forward in making carbon capture more economically viable for the cement industry.
Industrial policy
  Policy mandate: National "dual carbon" goals provide the strategic certainty for state-owned enterprises to make massive investments.
  State-led execution: The state-led model enables rapid resource mobilization and complex cross-sector integration, dramatically accelerating project timelines.
Qingzhou is the world’s first and largest cement oxy-fuel CC project
Decarbonization strategy
Energy efficiency: The Huaikan South production line project helped save 54M kWh/year and reduce CO₂ emissions by 160,000 tons/year.
Alternative fuels: The SPL clay calcination EPC project in France can reduce CO2 by 100,000 tons/year with the alternative fuel rate reaching 100%.
Low-carbon cement: High belite cement tech applied in the Jianwen project in Zhengzhou used proprietary tech to substitute clinker with other materials.
CCUS: The world’s largest industrial application of oxyfuel tech in Qingzhou used proprietary oxy-combustion tech to capture CO₂.
Observations
State-led mandates, financing, and permitting compressed projected delivery timelines from years to months.
Sinoma’s co-development of capture, power supply, and CO2 utilization improves project economics and reduced risk.
Oxy-fuel combustion was viable at this scale through national decarbonization targets and industrial policy support.
Sinoma’s case demonstrates how state-owned enterprises can mobilize capital, coordinate infrastructure, and scale CCUS in the cement sector.

## Slide 34: Fortera’s ReCarb technology uses mineral recarbonation to produce SCMs from captured carbon
products
process
Sources: Pitchbook, Fortera (2025); Fortera Global, ReCarb plants (2024); Global Cement, Low-CO2 inspired by nature (2021); Business Wire, Fortera opens first industrial green cement plant (2024).
Credit: Jessica Cong, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
Founded: 2019, California, U.S.
Total funding raised to date: $119 million
Limestone
Kiln
Calcium oxide (CaO)
CO₂ waste
The kiln is heated to a lower temperature of 900 to 1,100°C.
CO₂ is captured when limestone is heated during calcination and upcycled directly from the cement kiln.
The CO₂ is mineralized into a cementitious material that can be co-blended with Portland cement.
The product can be used as an SCM or a cementitious binder for preformed concrete materials such as bricks, blocks, or precast structures.
CCUS: Fortera
Technology
Fortera’s ReCarb process is a bolt-on solution that captures CO₂ released during clinker production and mineralizes it into carbonate-based cementitious material, which can serve as a supplementary cementitious material (SCM) or binder for precast products.
It forms stable calcium carbonate phases (e.g., vaterite and others), effectively locking in CO2 while reducing calcination emissions.
Current achievements
In April 2024, Fortera opened its first industrial green cement plant adjacent to CalPortland’s Redding, CA, facility, aiming to produce ~15,000 tons of ReAct low-carbon cement per year and capture ~6,600 tons of CO₂.

## Slide 35: Demand-side solutions offer significant additional opportunities for concrete emissions reductions across the value chain
1
Building design & construction
Concrete production
Cement production
Building usage & lifetime
Efficiency in concrete production
Shift from small-site batching to industrialized processes ensures better mix control.
Use of admixtures improves aggregate processing.
  Already applied in some countries.
Abatement potential: ~400 MtCO₂ per year by 2050.
Efficiency in design and construction
Material-efficient design, such as slab geometry, column spacing, and optimized strength, is reducing concrete demand.
Smart design systems reduce concrete demand.
Requires emissions to be a design parameter.
Abatement potential: ~800 MtCO₂ per year by 2050.
Recarbonization
Natural CO₂ uptake by concrete during lifetime.
12% to 23% of process emissions can be reabsorbed.
Requires access to demolition waste for maximum effect.
Abatement potential: ~250 MtCO₂ per year by 2050.
2
3
Sources: GCCA, Net-zero progress report (2024); GCCA, Concrete Future (2021); IVL methodology, CO2 concrete uptake (2021); Nature Communications, Benefits from cement carbonation (2024).
Credit: Soraya van Beek, Jessica Cong, Isabel Hoyos, Shailesh Mishra, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
Demand-side solutions
Opportunities to cut material demand and carbon emissions exist across the entire building lifecycle

## Slide 36: Smart design systems, such as 3D printing in concrete, can reduce material use by up to 50%
Use cases
3D printing has been used to develop innovative and sustainable solutions in emerging markets for:
  Modular solutions for low-cost housing.
  Resource-efficient buildings and schools.
  Concrete bases for wind turbines.
3D printing can reduce material use by up to 50% and reduce the time and cost for infrastructure projects.
3D printing innovations in concrete and construction
Source: Holcim (2020). Credit: Hoshi Ogawa, Sho Tatsuno, Jessica Cong, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
Scaling affordable housing in Africa:
14Trees, a joint venture between Holcim and British International Investment, launched Africa’s largest 3D-printed affordable housing project in Kilifi, Kenya, in 2021.
By 2023, the first 10 homes in the 52-unit complex were completed.
Taller wind turbines through 3D-printed concrete bases:
Holcim, GE Renewable Energy, and COBOD are collaborating to develop 3D-printed concrete bases for wind turbines up to 200 meters.
Traditionally bases — made from steel or precast concrete — are typically capped at ~100 meters, limited by the 4.5-meter transport diameter that makes larger bases uneconomical.
Enabling conventional concrete in 3D printing:
In 2022, Cemex and COBOD introduced D.fab, a proprietary admixture that allows 3D printing with standard ready-mix concrete.
The innovation reduces costs and material waste, making digital construction more accessible and commercially viable.
Demand-side solutions: 3D printing

## Slide 37: Cement Decarbonization Levers

## Slide 38
Decarbonizing cement requires coordinated action across technology, finance, and policy. While solutions are emerging — from CCUS in the Global North to LC3 in the Global South — adoption remains uneven due to structural and financial barriers.
  Most low-carbon levers remain pre-commercial, with limited real-world validation.
  Long certification cycles and strict durability standards slow uptake of new materials and blends.
  Knowledge sharing is limited, as proprietary technologies dominate the early innovation landscape.
Capital intensity and limited finance constrain scale-up.
  New cement plants require high CapEx at commercial scale; project finance options are scarce.
  The EU’s Innovation Fund has directed over €2.4 billion to cement and lime projects — primarily CCUS — but access is concentrated in Europe.
  Achieving a net-zero trajectory will require a 35% increase in investment by 2050, including $440 billion in enabling infrastructure (CCUS, SCM, and energy systems).
Fragmented value chains slow demand creation.
  70% to 75% of cement used ready-mix concrete with short procurement cycles.
  Government procurement (~50% of U.S. demand) is emerging as a key early market.
  Lack of unified standards and carbon accounting hinders product comparison.
Policy strength and technology pathways diverge by region.
  EU: Strongest mix (ETS, CBAM, Innovation Fund), but rising carbon costs challenge competitiveness.
  U.S.: Incentive-driven (IRA 45Q, IDP, Buy Clean) yet fragmented across states.
  Asia Pacific: Largest producer but under-regulated; LC3 and SCMs are favored as lower-cost decarbonization paths.
Cement Decarbonization Levers
Key messages
Credit: Hoshi Ogawa, Sho Tatsuno, Jessica Cong, Shailesh Mishra, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).

## Slide 39: Cement and concrete companies must work in tandem to decarbonize the construction value chain
Observations
~70% to 75% of cement goes into ready-mix concrete, prepared for roads, buildings, and other uses. This segment has strict standards and is hard to break into.
~10% to 15% of cement is used in precast concrete, which is mixed, molded, and cured before reaching the construction site. This segment can be more open to new players.
In the U.S., government procurement accounts for ~50% of concrete demand, giving public sector spending a significant role in market-side decarbonization and in driving demand for low-carbon materials.
Key roles for cement industry decarbonization across the value chain
Cement producers | Concrete producers | Concrete suppliers | Construction | End users
Implement emissions-reduction technologies like CCUS, alternative fuels, and kiln electrification. Replace clinker with SCMs (e.g., CCR, calcined clay). Improve thermal and electrical efficiency. | Reduce embodied carbon by lowering clinker factor in mixes. Use alternative binders and carbon-cured concrete. Shift to renewable energy sources. | Ensure wide availability of low-carbon concrete mixes. Reduce emissions in transport and batching operations. Lower building carbon footprint by optimizing design to codes and standards. Improve job site efficiency. Cut waste — 5% of concrete is returned unused. | Specify requests for low-carbon materials in tenders. Reduce waste and optimize structural design. Drive material efficiency across the project lifecycle. | Boost demand for low-carbon cement and concrete, specifically by public sector and governments. Shape design and material choices upstream. Build markets via long-term commitments and investments. Use policy and finance tools to enable innovation and decarbonization.
Sources: ACA, Roadmap to Carbon Neutrality (2025); FCA, Cement Value Chain (2024); RMI, Insights on cement industry’s net zero transition (2023); PCA, Roadmap to carbon neutrality (2024).
Credit: Beatrice Klein, Isabel Hoyos, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).

## Slide 40: Financing, operating, and stakeholder barriers are preventing the adoption of low-carbon cement and concrete
Financing
Stakeholder
Operating
High CapEx and limited financing options
Complex intermediaries
- Greenfield plants will be capital intensive. A new U.S. cement plant at 1+ MTPA commercial scale can require ~$0.5 billion to $1 billion in CapEx per deployment.
- Major investments are typically financed on the balance sheet with limited use of project finance.
Lack of long-term offtake agreements
Technological uncertainty
- Approximately 96% of all cement shipped goes through intermediaries.
- The value chain is highly fragmented at intermediary tiers between cement manufacturers and large buyers such as government procurement.
- Measures such as CCUS or alternative production methods for low-carbon cement have not been tested at commercial project scale in the U.S.
- Cement companies and investors will need to see technologies and business models de-risked before they pursue the substantial capital investments required for deployment at scale.
- Ready-mix companies and contractors purchase on an as-needed basis and are reluctant to commit to longer term offtake due to uncertainty about long-term demand amidst boom-and-bust construction market cycles.
- This makes it challenging to create a credible long-term demand signal for the scale-up of new technologies for low-carbon cement.
Lack of standard process and limited data
Risk aversion and long adoption cycles
- There is no single standard methodology to assess the embodied carbon of products, making it challenging to compare cements and concretes during a competitive procurement process.
- Lack of robust emissions data for specific inputs and production makes it challenging to conduct standardized environmental product declarations.
- The cement sector has a ~10- to 20-year adoption cycle for new blends and materials ― both from the long lead time to update standards and a long customer adoption cycle.
- Contractors, engineers, and ready-mix companies are risk-averse to adopting new technologies that may lead to budget and schedule overruns or safety risks.
Source: DOE Liftoff Report, Low carbon cement (2023).
Credit: Hoshi Ogawa, Sho Tatsuno, Jessica Cong, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).

## Slide 41: High CapEx and long horizons mean climate hard-tech startups must overcome technological and commercial ‘Valleys of Death’
Technological
Valley of Death
Commercial
Valley of Death
Observations
The two valleys are qualitatively different: the technological valley is a capital availability problem (negative IRR, no debt possible); the commercial valley is a risk-return mismatch (VC-level risk, infra-level returns).
Have elaborate development and testing process with high capital costs due to the hard-tech character of climate start-ups.
Capital scales ~5x to 10x at each stage; the largest absolute jump is to FOAK ($80M-$900M in a single step), when project finance is often not available yet.
The FOAK range ($100M-$1B) is the widest of any stage, reflecting sector variation.
Stages 1 and 3 show no IRR because they are funded from the corporate balance sheet: no standalone investment case yet.
"High teens to 25%" at FOAK reflects investor required rates, not realized returns — often a hurdle to obtaining investments.
Overcoming the first valley involves technological de-risking; the second requires proof of commercial viability and bankability of hard-tech solutions
Lab development
Pilot factory
Commercial-scale testing
FOAK1 plant
1
2
3
4
SOAK* plant
5
Product stage
Size of tech
1 small reactor
Multiple small reactors (e.g., 5x)
1 big reactor
Multiple big reactors (e.g., 20x)
Multiple big reactors
(e.g., 100x)
Proof of concept
Technology
Technical scalability
Commercial size technology
Commercial scalability and profitability
Commercial returns
Similar to FOAK but lower unit costs
Capital costs2
$1M-$20M
$5-$40M
$20-$100M
$100M-$1B
Expected
IRR
n/a
Negative IRR
n/a
High teens to 25%
n/a
System layout
Small system, testing technology
Integrated system with real process conditions
Larger engineering validation
Full integrated commercial plant
Replicated commercial plant
Deep Dive: FOAK Valleys of Death
1FOAK = first of a kind; SOAK = second of a kind. 2Capital costs refer to construction CapEx only; excludes OpEx, financing costs, and pre-FID development expenditure.
Sources: DOE, Learning from Case Studies: Financing and Development Approaches from Recent First-of-a-Kind Projects (2024); Sightline Climate, Meet the FOAK folks (2025); Extantia Capital, The FOAK Question: Essential Insights for Financing and Planning First-Of-A-Kind plants (2023).
Credit: Soraya van Beek, Isabel Hoyos, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).

## Slide 42: Capital efficiency key to overcoming technological Valley of Death; risk transfer across value chain key for commercial valley
Technological
Valley of Death
Commercial
Valley of Death
Reduction of capital needs by keeping team light and using existing equipment and materials (not reinventing every step in process).
Partnerships without equity, to develop pilot scale and establish first relationships for offtake agreements (hyperscalers often have the capital and risk appetite).
Government grants/loans, which should be politically agnostic (e.g., independence rather than climate).
Offtake agreements, to prove demand to secure potential project finance.
Tailored niche product instead of diversification (e.g., high-quality iron instead of high-volume steel)
Integration in established value chain with experienced partners for supply and construction.
Government grants and loans.
Observations
The technological valley solutions are primarily about capital efficiency: reducing what you need to spend; the commercial valley solutions are about risk transfer: shifting risk onto counterparties (offtakers, value chain).
Government grants are equally critical at the commercial valley: DOE/EU funding has been an enabler of FOAK project debt in recent cases (e.g. Stegra, LanzaJet).
"Tailored niche product" is a highest risk commercial strategy: It narrows the customer base, but protects margin if it works.
High-risk construction often leads to companies turning to in-house development.
The two solution sets are sequentially dependent.
Climate-tech startups must de-risk demand and often leverage public, concessional, or philanthropic capital to finance FOAK* commercial plants
Bench-scale testing
Pilot factory
Commercial-scale testing
FOAK* plant
SOAK* plant
1
2
3
4
5
Climate-tech start-ups are forced to self-develop and build their own plants because unproven technology and high construction risk make it impossible to find a licensing partner; only once commercial viability is demonstrated can they transition to the higher margin role of equipment provider or licensor.
Deep Dive: FOAK Valleys of Death
1FOAK = first of a kind; SOAK = second of a kind. 2Capital costs refer to construction CapEx only; excludes OpEx, financing costs, and pre-FID development expenditure.
Sources: DOE, Learning from Case Studies: Financing and Development Approaches from Recent First-of-a-Kind Projects (2024); Sightline Climate, Meet the FOAK folks (2025); Extantia Capital, The FOAK Question: Essential Insights for Financing and Planning First-Of-A-Kind Plants (2023).
Credit: Soraya van Beek, Isabel Hoyos, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).

## Slide 43: Other industries with high CapEx and long horizons underscore the need for structural mechanisms to overcome Valley of Death
 | Solar 1.0 | Pharmaceuticals & Biotech | Defense & Aerospace
Description of Funding Challenge | Until 2000s, solar panels were uncompetitive vs. fossil fuels. Manufacturers had no independent buyers at utility scale. Government R&D alone couldn't create commercial demand. | Pharma R&D costs between $0.3B and $2.6B per drug. 10- to 15-year timeline ~90% failure rate Biotech startups burn cash for years pre-revenue, with no guarantee of approval. | Major defense developments cost $10B to $50B+ per platform. 10- to 20-year development Companies often have only a single buyer (government).
Solution Approach to Valley of Death | Government "feed-in tariffs“ guaranteed 20-year revenue, converting unproven tech into bankable assets. Manufacturers like First Solar and SunEdison built their own first utility-scale plants to prove the technology. Learning curve showed that costs fell ~20% to 24% per doubling of capacity. | FDA phase gates (I → II → III) create staged value inflection points, each unlocking new investor classes. Big Pharma acquires/licenses at each gate. NIH funds ~$47B/year in early research. Risk becomes tradeable. | Government is the customer and the co-developer. Cost-plus contracts eliminate financial risk during R&D. Multi-decade procurement guarantees revenue before production
Context Similarity | High | Medium | Medium
Learnings for Climate Tech | Long term off-take guarantees foster “bankability.” | Structured de-risking steps needed to unlock new capital classes. | Government must recognize climate change mitigation as national security objective.
Sources: DOE OECD, Learning from Case Studies: Financing and Development Approaches from Recent First-of-a-Kind Projects (2024); U.S. GAO, F-35 Sustainment (2021); CBO, Research and Development in the Pharmaceutical Industry (2021); Bolinger et al., Levelized cost-based learning analysis of utility-scale wind and solar in the US (2022); Jones and Bouamane, A Business History of Solar Energy (2012).
Credit: Paul Greitemann, Soraya van Beek, Isabel Hoyos, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
Deep Dive: FOAK Valleys of Death

## Slide 44: Investment capacity and infrastructure drive CCUS in Global North; clay reserves and capital constraints drive LC3 in South
North America and the EU account for 92% of stated capacity from announced cement CCUS projects.
High capital needs and strong policy support (e.g., U.S. 45Q tax credit) drive CCUS deployment in high-income countries.
Existing oil and gas infrastructure in developed markets (e.g., pipelines, storage facilities, geological data) enable faster rollout. For example, Norway’s Northern Lights project uses existing North Sea oil infrastructure to store CO2..
Cement CCUS capacity1, global distribution, Dec. 2024
Clay calciner capacity1, global distribution, Dec. 2024
<1%
1-3%
3-5%
5-10%
10-15%
15-20%
<1%
1-3%
3-5%
5-10%
10-15%
15-20%
1 Expected at full operation based on stated disclosed carbon capture capacity for CCUS and stated disclosed installed capacity for clay calciner.
Source: GCCA and LeadIT, Green Cement Technology Tracker (2024).
Credit: Adele Teh, Isabel Hoyos, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
Africa accounts for 44% of stated capacity from announced clay calciner projects.
Clay calcination kilns are less capital intensive and easily integrated into existing cement plants than CCUS installations, making them a more attractive option for countries with limited industrial investment capacity.
Many developing countries have abundant clay reserves but rely on imported clinker due to the scarcity of high-grade limestone. Clay-based alternatives offer a cost-effective solution to meet rising cement demand amid rapid urbanization in developing countries.

## Slide 45: A broad range of policy instruments have been implemented to decarbonize cement manufacturing
Sources: WEF, Industry NZ tracker (2023); EU, Innovation Fund (2024); EU, Net-Zero Industry Act (2024); EU, ETS (2024); ICAP, California ETS (2024); EU, CBAM (2024); Office of Sustainability, Federal Buy Clean Initiative (2024); S&P, IRA 45Q (2023); CATF, CCfDs (2023); DOE, Industrial Demonstrations Program (2023). Credit: Hoshi Ogawa, Sho Tatsuno, Jessica Cong, Shailesh Mishra, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
Enablers | Policy type | Policy instrument | Key examples | Impact
Risk management | Risk-sharing | Financial certainty to innovators (through subsidy and incentives) | EU Carbon Contracts for Difference U.S. DOE’s Industrial Demonstration Program | Provides financial certainty to innovators by sharing investment risks in early-stage low-carbon technologies, incentivizing adoption and de-risking the transition to decarbonization solutions.
Technology | Incentive- based | R&D direct funding | EU Innovation Fund | $800 million funding for six cement CCUS projects in the EU.
 |  | Supporting regulations | EU Net-Zero Industry Act | Strengthens regulations and creates an enabling environment to boost CCUS technology development and stimulate investments; currently in the proposal stage.
 | Market- based | Carbon price | EU ETS California ETS China ETS (announced, not formalized) | Incentivizes cement producers to reduce emissions.
 |  | Border adjustment tariff | CBAM (pending implementation) Prove It Act (under discussion) | Emission-intensive cement exporters to the EU face a cost escalation of up to 100%; needs to be complemented by transparent and carbon accounting standards.
Demand | Incentive- based | Green public procurement (GPP) | GPP concrete product policies in Germany, the Netherlands, the UK, and Sweden Federal Buy Clean Initiative in the U.S. Key cement producers as IDDI members (UK, India) | Creates a viable market for low-emission cement through GPP commitments.
 | Mandate- based | Building/end-use product codes and standards | Embodied carbon limit policies in the Netherlands, Sweden, France, and Germany U.S. General Services Administration low embodied-carbon concrete standards in the U.S. | Provides a clear market signal to low-emission cement production.
Infrastructure | Incentive- based | CCUS infrastructure direct funding | Public funding of CCUS hubs in the EU CCUS hubs provision under Bipartisan Infrastructure Law | Over $6 billion committed to develop CCUS hubs in the U.S. and EU.
Capital | Incentive- based | Tax credits/subsidies | CCUS tax credits under IRA and OBBBA | 20% to 30% reduction in costs to deploy CCUS in cement plants.

## Slide 46: U.S., China, and EU + UK have deployed policies across the full carrots-sticks spectrum to incentivize cement decarbonization
2023: 71 MtCO2 World Rank: 3rd
Push
Improve project economics of cement decarb tech (credits, grants, concessional finance).
Pull
System
enablers
Penalize
Prohibit
Incentivize demand via procurement, disclosure, or embodied carbon rules.
Remove barriers via standards, codes, or infrastructure, to allow for new materials and supply chains.
Internalize externalities by raising costs or removing negative existing incentives.
Legal bans or caps on fuels, clinker, or emissions.
IRA 45Q tax credit for CCS since 2023, preserved under OBBBA.
Innovation Fund: 16 cement projects have been funded.
Carbon CfD pilot.
Green Credit Guidelines (updated 2021). Banks prioritize lending to green investments including green cement.
Buy Clean (federal/state) in 2021.
Public procurement guarantees demand. Federal canceled in 2025.
National Embodied Carbon Disclosures (e.g., France RE2020) binding since 2021. Creates demand for verified low-carb cement.
GB/T Green Building Code (MOHURD ’17+, revised ’20). Green materials in public projects. Pulls low-carb cement.
States’ DOT adoption of ASTM C1157 (Performance Cement Spec). Removes prescriptive clinker limits.
EN 197-5 Standard – CEN 2021. Active. Approves calcined clay (LC3) blends, enables clinker substitution.
GB 175-2023 and related SCM specs (GB/T 1596; GB/T 18046) legally define types and allow lower-clinker compositions.
California Cap-and-Trade Program (CARB, since 2013). Impact: Adds ~$2 to $35/tCO₂ to clinker cost.
RGGI C&T: $1.5B revenues in ’24.
EU ETS Phase IV and CBAM phase-in 2023-26. Tightens free allocation; border tariff raises cost of carbon-intensive imports.
National ETS expansion to cement; first compliance end of 2025. Absolute caps signaled for 2027.
Colorado DOT GWP caps for cement and concrete, Jan. 1, 2025; applies to projects with construction on or after July 1, 2025.
UK coal phase-out (BEIS, binding 2025). Cement kilns must shift away from coal fuels.
No new clinker capacity and strict capacity replacement (2024). Tougher replacement ratios (e.g., ~2:1 in air-polluted regions).
2023: 40 MtCO2 World Rank: 5th
2023: 718 MtCO2 World Rank: 1st
United States
EU and UK
China
Sources WEF, Industry NZ tracker (2023); EU, Innovation Fund (2024); EU, Net-Zero Industry Act (2024); EU, ETS (2024); ICAP, California ETS (2024); EU, CBAM (2024); GPP Pledge (2023); Office of Sustainability, Federal Buy Clean Initiative (2024); S&P, IRA 45Q (2023); EU; CCfDs (2024); DOE, Industrial Demonstrations Program (2023); Chinese Standards, Common Portland cement (2023); Global Carbon Atlas, Carbon Emissions (2023); ICAP, China ETS (2024); Reuters, China’s bank to extend carbon lending tool (2024); Colorado DOT, Buy Clean Colorado Act (2025); ICAP, USA - (RGGI) (2025). Credit: Nicolas Herrera Isaza, Isabel Hoyos, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
Policy type
Carrots
Sticks
Neutral

## Slide 47: EU + UK and China are tightening restrictive policies; U.S. is pulling back on incentive-based support
Chart: 
| 4 | 2 | 2.97 | 2.1 | 2 | 2.1
 | 4.6 | 4 | 3.1 | 2 | 1.2 | 1.2
 | 4.6 | 4 | 3 | 2 | 2
 | 4.6 | 4 | 2.9 | 2 | 1.2
45Q+IDP (F)
ASTM C1157 (S)
ETS (S)
GWP limits (S)
SB 596 (S)
Inn. Fund (R)
RE2020 (C)
EN197-5
ETS (R)
CBAM
Retrofit Fund
Green materials
SCM specs
ETS
Rest. clinker cap
Buy Clean (S)
Unbalanced and mixed landing zone
Mid-balanced and
mixed landing zone
Effective balance &
stronger landing zone
China’s mix features strict capacity caps (1.8B ton) but low carbon prices and diffuse financing.
Low direct funding, but new construction standards permit SCMs.
Strong national plans target 30% of cement capacity to reach benchmark energy efficiency1 by 2025.
ETS now covers cement. Price ~$13 per ton.
New ambitious NDC → outlook is positive.
Lean heavily on sticks; low balance score but high strength.
Carbon prices around €79/t.
CBAM (’26) closes carbon leaks.
Innovation Fund just covered 16 cement projects for ~€2.4B vs. ~€180B in revenue for ETS.
Uneven lower clinker content standards adoption (EN197-5).
Strengthening at a slower pace.
1 States include California, Oregon, Washington, Connecticut, Delaware, Maine, Maryland, Massachusetts, New Hampshire, New Jersey, New York, Pennsylvania, Rhode Island, and Vermont.
Sources: WEF, Industry NZ tracker (2023); Climate Bond Initiative (2023); EU, Innovation Fund (2024); EU, Net-Zero Industry Act (2024); EU, ETS (2024); ICAP, California ETS (2024); EU, CBAM (2024); GPP Pledge (2023); Office of Sustainability, Federal Buy Clean Initiative (2024); S&P, IRA 45Q (2023); EU; CCfDs (2024); DOE, Industrial Demonstrations Program (2023); Chinese Standards, Common Portland cement (2023); Global Carbon Atlas, Carbon Emissions (2023); ICAP, China ETS (2024); Reuters, China to extend carbon lending (2024); Colorado DOT, Buy Clean Colorado Act (2025); C2ES, US state carbon pricing (2025); Global Cement, EU funds 14 projects (2025); EU, ETS (2025); China Briefing, China’s CO2 reduction plan (2024); Climate Bonds, China’s green finance catalogue (2025). Credit: Nicolas Herrera Isaza, Isabel Hoyos, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
U.S.: Carrots being removed, few and weak sticks
EU + UK: Strong sticks, need stronger incentives
China: Refreshed ambitious NDC
U.S.
EU + UK
China
Relative strength
Moderate mix of carrots and sticks. Relative to the EU and China, the U.S. offers more carrots and puts less pressure on companies.
Large push incentives (e.g., 45Q $85) tCO2e + IDP) support limited number of projects.
Carbon pricing is limited to a few states (i.e., 13 states1) ~$30/tCO₂.
Outlook relaxes policies’ strength.
Medium
High
Low
S: State; F: Federal; R: Region; C:Country
Carrots
Sticks
Neutral
Outlook

## Slide 48: EU incentivizes decarbonization through ETS, CBAM, and public funding; push, protect, and pull mechanisms to that end
EU policy tools to incentivize decarbonization
Protect leakage
CBAM
ETS
Public
funds
Push costs
Cement/concrete
stakeholders
Close the market gap
Collect revenue
Collect revenue
Distribute subsidies and incentives
1
2
3
Primary carbon pricing mechanisms are pushing costs to emitters.
With free allowances starting to phase out in 2026 and falling to 0% in 2034, carbon prices are expected to surge.
Costs may increase 80% by 2034 for cement companies.
Program significantly strengthened since ETS Phase I through tighter caps, reduced free allocation, and structural reforms.
Market Stability Reserve (MSR, 2019) adjusts allowance supply to limit surplus and stabilize prices.
Aims to avoid carbon leakage due to imports coming from places with lower or no carbon costs (taxes or ETS).
Applied to certain imported goods, including cement.
Introduced originally in 2023. The levy phase-in will start in 2026 and be fully operational in 2034.
Up until 2023, member countries were expected to allocate at least 50% of ETS auctioning revenues toward climate and energy. In 2024, that expectation increased to 100%.
REPowerEU and the EU Innovation Fund are among the programs whose revenues are being directed toward decarbonization.
EU Emission Trading System (ETS)
EU Carbon Border Adjustment Mechanism (CBAM)
EU Public Funding
1
2
3
Deep dive: EU policy

## Slide 49: As EU ETS free allowances phase out, carbon is projected to represent ~30% to 50% of cement costs by 2034
Even in a conservative scenario, total allowance costs to the cement industry will see a sharp increase by 2034
Total cement costs could increase by ~50% to 100% by 2034 due to carbon pricing alone
Deep dive: EU policy
Assumptions: Emissions intensity 0.57 tCO2e/t cement as benchmark; stable cement consumption (production-exports+imports) at 160 Mt/year
Sources: CKI analysis; BCG, Decoding ETS and CBAM (2025); European Environment Agency, Use of EU ETS revenue (2024).
Credit: Nicolas Herrera Isaza, Isabel Hoyos, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
Chart: 
 | 0 | 53.34 | 216.79 | 543.69 | 1360.94 | 3060.82 | 3878.07 | 4695.32 | 5512.57 | 6427.89
 | 0 | 15.24 | 61.94 | 155.34 | 388.84 | 874.52 | 1108.02 | 1341.52 | 1575.02 | 1836.54
 | 0 | 15.24 | 61.94 | 155.34 | 388.84 | 874.52 | 1108.02 | 1341.52 | 1575.02 | 1836.54
 | 0 | 15.24 | 61.94 | 155.34 | 388.84 | 874.52 | 1108.02 | 1341.52 | 1575.02 | 1836.54
0
2025
2026
2027
2028
2029
2030
2031
2032
2033
6,428
2034
99
5,684
11,938
70-90 €/EUA
90-110 €/EUA
110-130 €/EUA
ETS total allowance costs scenarios for cement industry, € million
Incremental carbon pricing impact over cement costs, €/t of cement
Chart: 
 | 37.1721 | 37.1721 | 37.1721 | 37.1721 | 37.1721
 | 0.3311 | 3.3749 | 18.9995 | 29.1454 | 39.9
 | 0.0946 | 0.96425 | 5.4284 | 8.3273 | 11.4
 | 0.0946 | 0.96425 | 5.4284 | 8.3273 | 11.4
 | 0.0946 | 0.96425 | 5.4284 | 8.3273 | 11.4
80
2026
80
2028
80
80
2032
80
2034
.
81
86
115
134
154
2030
+40
+74
Base Cost
70 €/EUA
90 €/EUA
110 €/EUA
130 €/EUA
0.4-1%
4-7%
20-30%
27-40%
33-50%
%
Carbon cost share in total cement cost

## Slide 50: EU high cement prices are mainly driven by energy costs but show a correlation with the free allowances decrease from 2017 to 2021
Chart: 
 | 100.35 | 99.8 | 99.5 | 99.3 | 101 | 105 | 107.7 | 110.75 | 134 | 161.5 | 160
 | 129718797 | 128687449 | 128559709 | 124500074 | 121336487 | 120561372 | 117980876 | 97817636 | 98161847 | 98369683 | 94251719
 | 119395723 | 117839821 | 118290681 | 120961789 | 122684183 | 122232444 | 115510891 | 112622944 | 105688844 | 95734048 | 91232339
107.7
2020
110.8
97.8
112.6
2021
134.0
2016
100.4
2023
129.7
2024
119.4
2014
2015
2017
101.0
121.3
122.7
2018
2022
105.0
120.6
122.2
2019
+1.7%
+4.0%
+2.6%
+2.8%
Observations
In 2021, for the first time since ETS started, free allowances for cement were below the industry’s total emissions.
  Before the benchmark adjustment, cement companies were able to make profits from the free allowances they were given.
  In 2018, ETS primary market prices were on average at €15.5 per tCO2e, but in the same year, prices reached almost €25 per tCO2e — a historic maximum.
At the same time, cement prices increased by ~2.8% per year, which meant a jump of ~11.5% in four years.
While there was already a decreasing trend coming from 2016, 2017 through 2021 saw a 40% contraction in cement exports and 3x growth in imports.
EU ETS cement free allowances vs. cement emissions vs. cement prices, million tCO2e, €/t of cement
Deep dive: EU policy
Price
FA
Cement emissions
ETS sticks likely contributed to an increase in cement prices.
FA phase-out + CBAM phase-in will likely keep cement prices high…
…if low- or positive-cost abatement solutions are not supported (i.e., balancing carrots).
1 Cement companies were able to sell free allowances and make a profit of around €2 billion between 2008 and 2015. The ETS has since significantly tightened, leaving little to no room.
Sources: CEMBUREAU, EU cement industry trade statistics (2025); Trading Economics, EU producer prices: manufacture of cement (2025); Global Cement, EU funds 14 cement projects (2025); Global Cement, EU Innovation Fund (2025); Carbon Market Watch, Cement pollution windfall from EU ETS (2016); WWF, Clean industrial revolution in Europe (2025); EEA, EUU ETS data viewer, (2025); International Carbon Action Partnership (2025).
Credit: Nicolas Herrera Isaza, Isabel Hoyos, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).

## Slide 51: ETS revenues have reached €180B since 2013; of that, just ~€31B has been allocated to EU’s Innovation and Modernization funds
In 2024, EU ETS collected €38B as carbon prices grew and allowances tightened …
… but only 17% of cumulative revenue has gone to IF1 and MF2, which earmark EU investments for climate3
Chart: 
 | 3.1 | 2.8 | 4.3 | 3.4 | 4.9 | 12.6 | 14.1 | 14.4 | 25 | 29.7 | 33 | 38.8
 | 3.1 | 5.9 | 10.2 | 13.6 | 18.5 | 31.1 | 45.2 | 59.6 | 84.6 | 114.3 | 147.3 | 186.1
2013
2014
2015
2016
2017
2018
2019
2020
2021
2022
147.3
2023
2024
12.6
14.1
Cumulative revenue
Annual revenue
EU ETS revenues, € billion
Innovation Fund and Modernization Fund grants and investments, € billion
Chart: 
 | 0.36 | 0.36 | 1.7 | 7.05 | 13.58 | 23.98 | 19.2
 | 0.9 | 4.1 | 4.7 | 5.8 | 3.7 | 12.28
 | 0.44 | 1.25 | 1.83 | 4.6 | 3.8 | 0
2020
0
1
2021
1
2022
2
2023
2024
2025
Cumulative I & M Funds
1
5
7
11
8
31
IF
MF
Chart: 
 | 16.9264
 | 83.0736
Cumulative ETS Revenue
186.1
1 EU Innovation Fund. 2 EU Modernization Fund. 3 Most revenue goes to member countries, which are required to allocate it toward climate purposes. Since 2024,100% of the revenues given to countries should be used for climate action, including social costs of climate change.
Sources: EU, Innovation Fund (2024); EU, Modernisation Fund (2024); EEA, Use of EU ETS revenues (2024); European Commission, Auctioning of allowances (2025).
Credit: Nicolas Herrera Isaza, Isabel Hoyos, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
Deep dive: EU policy

## Slide 52: Cement contributed little to ETS revenues but received ~20% of the Innovation Fund’s contributions — its greatest beneficiary
EU GA1 IF contributions, € billion
99.9% of funds target CCUS projects, one of the highest cost solutions for cement decarbonization
Deep dive: EU policy
 | 16 | €152,3
 | 34 | €63,6
 | 23 | €73,8
 | 14 | €75,5
 | 14 | €65,1
 | 15 | €58,8
 | 8 | €93,7
 | 93 | €25,5
Chart: 
 | 2437289247.61 | 2162976840.76 | 1698114884.24 | 1057652887.87 | 912085876.71 | 883241458.78 | 749738120 | 2370934573.25
Cement & lime
Hydrogen
Chemicals
Other
Manufacturing components for RE or BESS
Refineries
Iron & steel
Other 18
2.4
2.2
1.7
1.1
0.9
0.9
0.7
2.4
# projects | Avg. €/project
1 GA: Grant agreements.
Source: EU, Innovation Fund (2024).
Credit: Nicolas Herrera Isaza, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
Chart: 
 | 26.3448 | 4.5 | 4.4
CCUS
SCMs
Fuel substitution
2,428.0
Innovation Fund and Modernization Fund grants and investments, € million
Germany | €686,6 |  | 
France | €398,6 |  | 
Greece | €358,3 |  | 
Belgium | €230,0 |  | 
Poland | €228,2 |  | 
Denmark | €220,1 |  | 
Bulgaria | €189,7 |  | 
Croatia | €116,9 |  | 
Spain |  | €4,4 | €4,5
Higher allocations due to large pipeline of ETS-exposed, investment-ready industrial projects

## Slide 53: New York State's Buy Clean Concrete guidelines mandate environmental standards (EPDs) and set GWP limits for concrete
New York State’s Buy Clean Concrete guidelines
Minimum emission limits for concrete
Deep dive: U.S. policy
Section | Explanation
Environmental standards (EPDs) | Mandatory Environmental Product Declarations (EPDs) are required for all concrete mixes starting Jan. 1, 2025. These guidelines quantify the environmental impact of products over their lifecycle.
Who does this affect? | State agency projects over $1 million. Department of Transportation projects over $3 million.
Emission limits (GWP) | Specifies GWP (global warming potential) limits for concrete, expressed in CO2e (carbon dioxide equivalent), with adjustments planned post-2026.
Timeline | Phase 1 (2024): Voluntary GWP and EPDs Phase 2 (2025-2026): Mandatory compliance and certification Phase 3 (post-2026): Revised GWP limits
Compressive strength (PSI) | Maximum emission limits (kg CO2e per cubic yard)
0 – 2500 | 275
2501 – 3000 | 302
3001 – 4000 | 360
4001 – 5000 | 434
5001 – 6000 | 458
6001 – 8000 | 541
Source: NYS, Buy Clean Concrete Guidelines (2023).
Credit: Hoshi Ogawa, Sho Tatsuno, Shailesh Mishra, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).

## Slide 54: The New York cement supply chain faces regulatory constraints, high energy consumption, logistics costs, and market pressures
Supply chain stages and pain points
Deep dive: U.S. policy
Environmental degradation.
Regulatory constraints on land use.
Fluctuating quality of raw materials.
High energy consumption and carbon emissions, especially in clinker production.
Aging infrastructure, leading to inefficiencies.
Compliance with stringent environmental regulations.
Logistics costs, impacted by fuel prices and infrastructure limitations.
Emissions from transportation.
Supply chain disruptions.
Competitive market pressures.
Sensitivity to economic cycles affecting construction demand.
Navigating state-specific requirements like New York’s low embodied carbon concrete regulations.
Ensuring product performance under diverse environmental conditions.
On-site storage and handling issues.
Adapting to innovative building practices and materials.
Extraction & Raw Materials
Manufacturing
Distribution
Sales & Market Demand
End Use & Application
Source: NYS, Buy Clean Concrete Guidelines (2023).
Credit: Hoshi Ogawa, Sho Tatsuno, Shailesh Mishra, Isabel Hoyos, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).

## Slide 55: Delivering a net-zero future requires a 35% increase in investment to develop necessary enabling infrastructure
Cumulative investments, projected 2022 to 2050
Chart: 
 | 1050 | 980 | 553.8
 | 440 | 383.4
 | 28.4
 | 255.6
 | 14.2
 | 184.6
2022 base scenario
2050 net-zero scenario
13%
1%
18%
2%
27%
39%
2050 net-zero scenario, by investment category
Investment in enabling infrastructure (beyond the plant’s boundaries)
Investment within the concrete and cement sector (within the plant)
Clinker-making capacity
Carbon capture equipment
SCMs
Electricity infrastructure
Hydrogen infrastructure
CCUS infrastructure
$1,420 (1,100 to 1,950)
$1,420 (1,100 to 1,950)
$1,050 (700 to 1,300)
+35%
-7%
Sources: Mission Possible, Making net-zero concrete and cement possible (2023); GCCA, Concrete future: Roadmap to net zero (2021).
Credit: Shailesh Mishra, Jessica Cong, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
Billions of dollars, midpoint

## Slide 56: Different roadmaps consider efficiency, material substitution, and CCUS as key decarbonization levers, with CCUS abating ~36%-50%
Comparison of global cement and concrete decarbonization levers by 2050
Chart: 
 | 47 | 44 | 42.5 | 24 | 20.39
 | 37 | 36 | 38 | 7 | 56.93
 | 16 | 9 | 12.5 | 45 | 23.44
 | 11 | 7 | 7 | 19.18
 | 17
IEA
GCCA
MPP
45%*
24%
McKinsey
CEMBUREAU
120%
Europe
Energy efficency & alternative fuels
Material substitution
CCUS
Material efficiency
Unabated emissions
Global
Total abatement exceeds 100% because the roadmap includes carbon removal strategies (e.g., CCUS, carbonation) that go beyond reducing emissions, enabling net-negative emissions (-131 kg CO₂/t) by 2050.
Percentage share of CO2 emissions abated by key levers
Sources: DOE, Pathways to Commercial Liftoff (2023); GCCA, Concrete future: Roadmap to net zero (2021); McKinsey, Zero-carbon cement (2020); ClimateWorks Foundation (2021); CEMBUREAU, From Ambition to Deployment (2024).
Credit: Beatrice Klein, Isabel Hoyos, Shailesh Mishra, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).

## Slide 57
CKI Cement Team – Fellows and Alumni
Alumni
Current Fellows
Jessica Cong
Master of Business Administration
CKI Fellow
Hyae Ryung (Helen) Kim
PhD in Sustainable Development
Sho Tatsuno
Master of Business Administration
CKI Fellow
Shailesh Mishra
MPA in Development Practice
CKI Fellow
Adele Teh
Master of Business Administration
CKI Fellow
Nicolás Herrera Isaza
MS in Sustainability Management
CKI Fellow
Hoshi Ogawa
Master of Business Administration
CKI Fellow
Hassan Riaz
Master of Business Administration
CKI Fellow
Soraya van Beek
Master of Business Administration
CKI Fellow
Camilo Avilés
MS in Sustainability Management
CKI Fellow

## Slide 58
Shiho Kawashima
Associate Professor of Civil Engineering and Engineering Mechanics, Columbia University
Kimberly E. Kurtis
Associate Dean of Faculty Development & Scholarship, Engineering, Georgia Institute of Technology
CKI Cement Staff, Faculty, and Advisors
Pia Doris Morrow
M.S. in Sustainability Management
Staff Associate
pm3346@columbia.edu
Selen Bilgin Olmez
M.S. in Sustainability Management
Staff Associate sb5151@columbia.edu

## Slide 59: Appendix

## Slide 60: Blended cements partially replace clinker, reducing emissions with just minor changes to the production process or added costs
Limestone calcined clay cement (LC3): Leading blended cement
Observations
Blended cements partially substitute clinker with supplementary cementitious materials (SCMs).
Limestone calcined clay cement (LC3) is a leading blended cement offering a viable pathway to decarbonize the cement industry.
  LC3 has a clinker ratio of 0.5.
  Compared with ordinary Portland cement, it has 40% less CO₂ emissions and 25% lower overall costs.
  Lower processing temperatures: Calcining clay requires flame temperatures of 690-800⁰C, much lower than that required by traditional clinker.
Clinker-to-cement ratios vary considerably by region due to material availability and local regulations.1
1 In some countries, SCM substitution occurs during concrete manufacturing rather than cement manufacturing.
Sources: IFC, Strengthening Sustainability in the Cement Industry (2025); IEA, Cement (2023); Congressional Research Service, Cement (2023); IEA, Net Zero by 2050 (2021); RMI, Unleashing the Potential of LC3 (2023); International Cement Review, SCMs: Environmental and Qualitative Benefits (2022). Credit: Adele Teh, Hoshi Ogawa, Sho Tatsuno, Jessica Cong, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
Blended cements
Chart: 
 | 50 | 30 | 15 | 5
Clinker
Calcined clay
Limestone
Gypsum
Chart: 
 | 0.89 | 0.86 | 0.77 | 0.65
U.S.
Canada
Europe
China
Clinker-to-cement ratios vary considerably by region, latest available:
40% less CO₂ emissions
Enhanced durability and performance
25% lower overall costs
Accelerating global adoption

## Slide 61: Announced global cement clay calciner projects expected to reach 380 Mt per year at full capacity; Ghana leads with ~99% share
USA
Chart: 
 | 0
 | 0
 | 0
 | 0
 | 0
1
0
58
Stated clay calciner installed
capacity (Mt/year)
Global distribution of stated clay calciner installed capacity, project count and Mt/year, Dec. 2024
2
0
0
CAN
Chart: 
 | 0.15
 | 0
 | 0
 | 0
 | 0.15
1
0
0
0
CHN
Chart: 
 | 0
 | 0
 | 0
 | 0
 | 0
1
0
0
0
PER
Chart: 
 | 0.16936
 | 0
 | 0
 | 0
 | 0.16936
1
0
0
0
EU
Chart: 
 | 0.9
 | 0
 | 0
 | 0
 | 0.9
8
1
0
5
IND
Chart: 
 | 0
 | 0
 | 0
 | 0
 | 0
1
0
0
1
BRA
Chart: 
 | 0.7672
 | 0.001431
 | 0
 | 0
 | 0.76863
3
0
0
0
AGO
Chart: 
 | 0.3
 | 0
 | 0
 | 0
 | 0.3
1
0
0
0
World
Chart: 
 | 5.9906
 | 0
 | 1.46e-05
 | 0
 | 5.9906
1
7
27
0
Full scale, no. of projects
Demonstration, no. of projects
Pilot, no. of projects
Feasibility study, no. of projects
ARG
Chart: 
 | 0.2
 | 0
 | 0
 | 0
 | 0.2
1
0
0
0
BFA
Chart: 
 | 0.5256
 | 0
 | 0
 | 0
 | 0.5256
2
0
0
0
CIV
Chart: 
 | 0.6504
 | 0
 | 0.025
 | 0
 | 0.6754
2
0
0
0
CMR
Chart: 
 | 0.4
 | 0
 | 0
 | 0
 | 0.4
1
0
0
0
GHA
Chart: 
 | 0.77876
 | 0
 | 0
 | 0
 | 0.77876
2
0
0
0
OMN
Chart: 
 | 0
 | 0
 | 0
 | 0
 | 0
1
0
0
0
SAU
Chart: 
 | 0.7
 | 0
 | 0
 | 0
 | 0.7
1
0
0
0
COL
Chart: 
 | 0.45
 | 0
 | 0
 | 0
 | 0.45
1
0
0
0
Observations
Savings in cement and binders, including calcined clays, accounts for 11% of planned emissions reductions in the GCCA 2050 net-zero roadmap, which has been backed by 40 cement producers since 2021.
Africa accounts for 44% of stated capacity from announced clay calciner projects.
Clay calcination kilns are less capital intensive and easily integrated into existing cement plants — an attractive option for developing nations with limited industrial investment capacity.
Many developing countries have abundant clay reserves but rely on imported clinker due to scarce high-grade limestone.
Clay-based alternatives offer a cost-effective solution to meet rising cement demand amid rapid urbanization in developing countries.
Source: GCCA and LeadIT, Green Cement Technology Tracker (2024).
Credit: Adele Teh, Isabel Hoyos, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).

## Slide 62: Announced global cement CCUS projects >40 MtCO₂ per year at full capacity; EU leads with ~66% share
USA
Chart: 
 | 0.95
 | 0
 | 0.000876
 | 6.05
 | 7.0009
Observations
CCUS accounts for 36% of planned emissions reductions in the GCCA 2050 net-zero roadmap, which has been backed by 40 cement producers since 2021.
The roadmap targets 1,370 Mt of CO₂ captured by 2050.
North America and the EU account for 92% of stated capacity from announced cement CCUS projects.
High capital needs and strong policy support (e.g., U.S. 45Q tax credit) drive CCUS deployment in developed countries.
Existing oil and gas infrastructure in developed markets (e.g., pipelines, storage facilities, geological data) enables faster rollout.
For example, Norway’s Northern Lights project utilizes existing North Sea oil infrastructure to store CO2.
1
1
58
Expected stated capture capacity
at full operation, MtCO2/year
Global distribution of stated carbon capture capacity, project count and MtCO2/year, Dec. 2024
2
4
2
AUS
Chart: 
 | 0
 | 0.02
 | 0.1
 | 0
 | 0.12
0
1
0
1
CAN
Chart: 
 | 1
 | 1.5
 | 1
 | 0
 | 3.5
1
1
0
1
CHN
Chart: 
 | 0
 | 0.55
 | 0
 | 0
 | 0.55
0
5
0
0
COL
Chart: 
 | 0
 | 0
 | 0
 | 0
 | 0
0
0
0
1
EU
Chart: 
 | 7
 | 0.1
 | 0.025
 | 1.5
 | 8.625
30
5
3
7
IND
Chart: 
 | 0
 | 0.5
 | 0
 | 0
 | 0.5
0
1
0
0
JPN
Chart: 
 | 0
 | 0.001431
 | 0
 | 0
 | 0.001431
0
2
1
0
NOR
Chart: 
 | 0.4
 | 0.001431
 | 0
 | 0
 | 0.40143
1
1
0
0
GBR
Chart: 
 | 0.6
 | 0.001431
 | 0
 | 0.8
 | 1.4014
2
0
1
1
TWN
Chart: 
 | 0
 | 0
 | 0.55
 | 0
 | 0.55
0
0
0
2
World
Chart: 
 | 28.931
 | 2.6714
 | 1.6759
 | 8.35
 | 41.6283
17
15
35
9
Full scale, no. of projects
Demonstration, no. of projects
Pilot, no. of projects
Feasibility study, no. of projects
Source: GCCA and LeadIT, Green Cement Technology Tracker (2024).
Credit: Adele Teh, Isabel Hoyos, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).

## Slide 63: The EU Innovation Fund has invested in 16 cement projects for demonstration of innovative low-carbon technologies
Observations
In the EU, polluters have to pay for their greenhouse gas emissions via the Emissions Trading System (ETS).
The money raised via the EU ETS is reinvested into the Innovation Fund, one of the world’s largest funding programs for the demonstration of innovative low-carbon technologies.
As of September 2025, 16 out of 214 projects funded by the EU Innovation Fund (US$12.2 billion) are cement-related projects, totaling US$2.44 billion in investment.
Though all cement projects have different technology installations, they all have CCUS installation plans as part of the projects.
Number of projects EU Innovation Fund has invested in, 2025
Chart: 
 | 31 | 23 | 16 | 15 | 14 | 14 | 12 | 11 | 10 | 9 | 9 | 8 | 7 | 6 | 6 | 5 | 4 | 3 | 2 | 2 | 2 | 2 | 1 | 1 | 1
Hydrogen
Chemicals
Cement & lime
Refineries
Glass, ceramics, and construction
Other
Glass, ceramics, & construction materials
Components; renewable energy
Intraday electricity storage
Components; energy-intensive industries
Other energy storage
CO2 transport
Maritime
Solar energy
Wind energy
Hydro/ocean energy
Components; energy storage
Non-ferrous metals
Renewable heating/cooling
Geothermal energy
Pulp & paper
Use of renewable energy outside Annex I
Aviation
Renewable heating/cooling
Road transport
EU contribution by sector in 2025, billions EUR
Chart: 
 | 2.0429 | 1.6981 | 2.4373 | 0.88324 | 0.91209 | 1.0577 | 0.086757 | 0.31543 | 0.16553 | 0.46466 | 0.096099 | 0.74974 | 0.20239 | 0.023545 | 0.16461 | 0.15681 | 0.29368 | 0.029189 | 0.088 | 0.096099 | 0.008688 | 0.0053978 | 0.095 | 0.0075404 | 0.0715
Source: EU Innovation Fund, Innovation Fund Portfolio (2024).
Credit: Hoshi Ogawa, Ariela Farchi, Sho Tatsuno, Jessica Cong, Shailesh Mishra, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
EU policy

## Slide 64: GCCA’s net-zero roadmap cites CCUS and improved material efficiency as the key levers for decarbonizing the cement sector
Source: GCCA, Concrete future, roadmap to net zero (2021).
Credit: Shailesh Mishra, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
GCCA roadmap: Cement decarbonization levers by 2050
Chart: 
 | -2.5 | -2.5 | -3.83 | -2.99 | -2.56 | -2.21 | -1.8 | -1.61 | -1.37 | -1.37
 | -1.33 | -0.84 | -0.43 | -0.35 | -0.41 | -0.19 | -0.24
2020 emissions
1.33
BAU emissions increase
2050 emissions (BAU)
0.84
Efficiency in design and construction
0.43
Efficiency in concrete production
0.35
Savings in cement and binders
0.41
Savings in clinker production
0.19
Decarbonization of electricity
0.24
Recarbonation
1.37
CCUS
Cement industry emissions, 2020-2050, GtCO2

## Slide 65: ACA pathway expects CCUS and concrete mixture optimization to lead decarbonization, abating ~51% and ~26%, respectively
Source: American Cement Association, Roadmap to Carbon Neutrality (2024).
Credit: Shailesh Mishra, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
PCA carbon-neutrality levers, 2050
Chart: 
 | -100 | -95 | -69 | -66 | -51 | -51
 | -5 | -26 | -3 | -15
100%
2050 emissions
5%
Efficiency in concrete production
26%
Optimized concrete mixtures
3%
Reduced emissions in concrete transportation
15%
Savings in clinker production
51%
CCUS
Percentage share of CO2 emissions abated by measures

## Slide 66: CEMBUREAU's 2050 roadmap projects -131 kgCO2/t cement emissions through CCUS, clinker substitution, and circularity
Sources: CEMBUREAU, From Ambition to Deployment (2024).
Credit: Shailesh Mishra, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
Chart: 
 | 804 | 657 | 531 | 377 | 303 | 243 | 243
 | 126 | 154 | 74 | 60 | -131
1990
2021
Alternate binding materials and fuel switching
Clinker substitution and electrical efficiency
Optimized concrete mix
Construction carbonation
131
CCUS
2050 emissions
374
-131
120%
CEMBUREAU total process emissions, including downstream, 1990-2050
kg CO2 per ton of cement

## Slide 67: DOE's Industrial Decarbonization Roadmap highlights CCUS as a key lever reducing 65% of CO2 emissions for the U.S. market
1 Percent share of emissions abated by energy efficiency, electrification, and LCFFES, and alternate approaches.
Source: DOE, Industrial Decarbonization Roadmap (2022).
Credit: Shailesh Mishra, Hyae Ryung Kim, and Gernot Wagner. Share with attribution: Wagner et al., “Decarbonizing Cement” (16 July 2026).
DOE Industrial Decarbonization Roadmap emissions for U.S. cement manufacturing sector, 2015-50, MtCO2
Chart: 
 | -69 | -85.42 | -55.53 | -55.53
 | -29.89
2015
2050 emissions (BAU)
29.9
Others1 (energy efficiency, electrification, and LCFFES, and alternate approaches)
55.5
CCUS
69.0
85.4
35%
65%

## Slide 68: Emerging cement producing economies, China and India consider new processes alongside traditional decarbonization levers
Observations
CCUS dominates: The largest share of emissions abatement comes from CCUS in both countries — India (47%), China (40%) — signaling reliance on large-scale capture infrastructure.
India bets on innovation: Greater share in new processes (13% vs. 9% China) shows focus on tech upgrades.
Low impact from efficiency: Efficiency and alternative fuels remain limited (9% to 10%) in both pathways.
Share of CO₂ emissions abated by key decarbonization levers by 2050
Chart: 
 | 11 | 9
 | 18 | 16
 | 40 | 47
 | 9 | 10
 | 13 | 5
 | 9 | 13
11%
China
9%
India
New processes
Efficiency and
alternative fuels
Material substitution
CCUS
Lifecycle efficiency
Unabated emissions
ClimateWorks projections

## Slide 69: Glossary
BAU | Business as usual
CaCO3 | Calcium carbonate
CaO | Calcium oxide
CapEx | Capital expenditure(s)
CBAM | Carbon Border Adjustment Mechanism
CCUS | Carbon capture, utilization, and storage
CO | Carbon monoxide
CO2 | Carbon dioxide
CO2e | CO2 equivalent, using global warming potential as conversion factor
EBITDA | Earnings before interest, taxes, depreciation, and amortization
ETS | Emissions Trading System
EPD | Environmental Product Declarations
EU | European Union
FMC | Federal Materials Council
GCCA | Global Cement and Concrete Association
GPP | Green public procurement
RDF | Refuse-derived fuel
GSA | General Services Administration
Gt | Gigaton (billion metric tons)
GWP | Global warming potential
H2 | Hydrogen
H2O | Water
IDDI | Industrial Deep Decarbonization Initiative
IEA | International Energy Agency
IRA | Inflation Reduction Act
LCA | Lifecycle assessment
Mt | Megaton (million metric tons)
MTPA | Million tons per annum
NZE | Net-zero emissions
O2 | Oxygen
OpEx | Operational expenditure(s)
PCA | Portland Cement Association
RMC | Ready-mix concrete
SCM | Supplementary cementitious materials
SRF | Solid recovered fuel